**Modification of paint coatings by incorporation of organomontmorillonites**

**Kurenkov Viktor V.**

A.V. Topchiev Institute of Petrochemical Synthesis, RAS (TIPS RAS)**.** E-mail: viktorkur@yandex.ru

**Gerasin Viktor A.**

A.V. Topchiev Institute of Petrochemical Synthesis, RAS (TIPS RAS). E-mail : gerasin@ips.ac.ru

***Keywords:*** *organoclay, montmorillonite, polymer, nanocomposite, coating.* Production of polymer-aluminosilicate nanocomposites with layered silicate montmorillonite used as a nanoadditive is a prospective approach for development of polymer materials with improved properties, including polymer and paint coatings. The performance characteristics of alkyd coatings modified with organomontmorillonites Cloisite 15A, Cloisite 30B were characterized, the structure of organomontmorillonite in the composite coating was determined. The study shows that formation of intercalated nanocomposite leads to improvement of the performance characteristics of composite coatings. The positive effect of organomontmorillonite incorporation shows in cases of both pigmented and non-pigmented alkyd coatings.

**References**

1. Gerasin V.A., Antipov E.M., Karbushev V.V., Kulichikhin V.G., Karpacheva G.P., Talroze R.V., Kudryavtsev Y.V. New approaches to the development of hybrid nanocomposites: from structural materials to high-tech applications. Uspekhi khimii [Russian Chemical Reviews], v. 82, no. 4, p. 303-332. ( in Russ).

2. Bergaya F., Theng B. K. G., Lagaly G. (ed.). Handbook of clay science // Elsevier, 2011.

3. Heidarian M., Shishesaz M.R. Study on effect of duration of the ultrasonication process on solvent‐free polyurethane/organoclay nanocomposite coatings: Structural characteristics and barrier performance analysis. Journal of Applied Polymer Science. 2012, v. 126, no. 6, p. 2035-2048.

4. Malin F., Znoj B., Šegedin U., Skale S., Golob J., Venturini P. Polyacryl–nanoclay composite for anticorrosion application. Progress in Organic Coatings. 2013, v. 76, no. 10, p. 1471-1476.

5. Verma G., Kaushik A., Ghosh A.K. Comparative assessment of nano-morphology and properties of spray coated clear polyurethane coatings reinforced with different organoclays. Progress in Organic Coatings. 2013, v. 76, no. 7, p. 1046–1056.

6. Heidarian M., Shishesaz M. R., Kassiriha S. M., Nematollahi M. Characterization of structure and corrosion resistivity of polyurethane/organoclay nanocomposite coatings prepared through an ultrasonication assisted process. Progress in Organic Coatings, 2010, v. 68, no. 3, p. 180–188.

7. Dai C.F., Li P.R., Yeh J.M. Comparative studies for the effect of intercalating agent on the physical properties of epoxy resin-clay based nanocomposite materials. European Polymer Journal. 2008, v. 44, № 8, p. 2439–2447.

8. Kurenkov V.V., Gerasin V.A., Korolev Yu.M., Piryazev A.A., Mendeleev D.I., Dyachuk S.V. Polyethylene-aluminosilicate nanocomposites for pipeline protection coatings. Plasticheskie massy [Plastics], no 7-8. p. 53-60. ( in Russ).

9. Steele A., Bayer I., Loth E. Adhesion strength and superhydrophobicity of polyurethane/organoclay nanocomposite coatings. Journal of Applied Polymer Science, 2012, v. 125, no. S1.

10. Bagherzadeh M.R., Mousavinejad T. Preparation and investigation of anticorrosion properties of the water-based epoxy-clay nanocoating modified by Na+-MMT and Cloisite 30B. Progress in Organic Coatings. 2012, v. 74, no. 3, p. 589–595.

11. Piazza D., Baldissera A.F., Kunst S.R., Rieder E.S., Scienza L.C., Ferreira C.A., Zattera A.J. Influence of the addition of montmorillonite in an epoxy powder coating applied on carbon steel. Materials Research. 2015, v. 18, no. 5, p. 897–903.

12. Li J., Ecco L., Fedel M., Ermini V., Delmas G., Pan J. In-situ AFM and EIS study of a solventborne alkyd coating with nanoclay for corrosion protection of carbon steel. Progress in Organic Coatings. 2015, v. 87, p. 179-188.

13. Dai C.F., Li P.R., Yeh J.M. Comparative studies for the effect of intercalating agent on the physical properties of epoxy resin-clay based nanocomposite materials. European Polymer Journal. 2008, v. 44, no. 8, p. 2439–2447.

14. Gorrasi G., Tortora M., Vittoria V. Synthesis and Physical Properties of Layered Silicates/ Polyurethane Nanocomposites. Journal of Polymer Science: Part B: Polymer Physics. 2005, v. 43, p. 2454–2467.

15. Frounchi M., Dadbin S., Salehpour Z., Noferesti M. Gas barrier properties of PP/EPDM blend nanocomposites. Journal of membrane science. 2006, v. 282, № 1, p. 142–148.

16. Osman M.A., Rupp J.E.P., Suter U.W. Effect of non-ionic surfactants on the exfoliation and properties of polyethylene-layered silicate nanocomposites. Polymer. 2005, v. 46, no. 19, p. 8202–8209.

17. Stesyakov A.A., Gerasin V.A., Yakovleva A.V., Antipov A.E. Method of production of thin-dispersed clay material. RU № 2619622., B. № 14, 2017. ( in Russ).

18. Bakhov F.N., Cherkina U.Yu., Shtepa S.V. Method of production of organomodified montmorillonite with improved thermal stability (variants). RU № 2519174., B. № 16, 2014. ( in Russ).

**Degradable compositions based on polyvinyl chloride and bentonite**

**Volkova Kseniia**, PhD-student

assistant, Department of IT in the Fuel and Energy Industry, Saint Petersburg State University of Information Technologies, Mechanics and Optics. E-mail: volkova.kseniia@yandex.ru

​**Sitnikova Vera**, PhD

tutor, Department of IT in the Fuel and Energy Industry, Saint Petersburg State University of Information Technologies, Mechanics and Optics. E-mail: kresenka@gmail.com

**Sibirtsev Vladimir**, PhD

доцент, Department of IT in the Fuel and Energy Industry, Saint Petersburg State University of Information Technologies, Mechanics and Optics. E-mail: vs1969r@mail.ru

**Uspenskaya Maya**, Professor, DSc

Head of Department of IT in the Fuel and Energy Industry, Saint Petersburg State University of Information Technologies, Mechanics and Optics.

E-mail: mv\_uspenskaya@mail.ru

**Beluhichev Evgeniy**, PhD

Аспирант, Saint-Petersburg State Institute of Technology

Russia, 197101, St. Petersburg, Kronverkskiy pr., 49, lit. A.

E-mail: e.belukhichev@kpfilms.com

**Sivtsov Evgeniy**, DSc

Head of Department colloid chemistry, Saint-Petersburg State Institute of Technology

Russia, 197101, St. Petersburg, Kronverkskiy pr., 49, lit. A. E-mail: pjeka@yahoo.fr

***Keywords:*** *polyvinyl chloride, bentonite, composite material, degradation.*

Polymer composite films based on polyvinylchloride and bentonite of various concentrations have been studied. The influence of technological parameters of the process is studied: the proportion of reagents and the rolling time on the mechanical characteristics of PVC filled films. It is shown that the introduction of natural bentonite leads to the formation of filler agglomerates with dimensions of 30-120 μm, and the resulting films exhibit anisotropy of properties. It is shown that an increase in the rolling time to 10 minutes results in the thermal destruction of the polymer composite material. It has been demonstrated that the introduction of bentonite 1 wt.% Leads to the appearance of biodegradable properties of polyvinyl chloride films, while using 5% by weight of mineral filler, the overall degradability of the polymer materials being studied is due to mechano-degradability.

**References**

1. Nizamov R.K. Polyfunctional fillers for polyvinylchloride compositions for construction purposes. Building Materials, 2006, No. 7, pp. 68-70 (in Russ.).

2. Sedykh V.A, Zhuchkov A.V. Technical properties of packaging films on the basis of PVC. Vestnik Voronezh State University of Engineering Technologies. 2013, No. 2 (56), pp. 141-146 (in Russ.).

3. Sadat-Shojai M., Bakhshandeh G-R. Recycling of PVC wastes. Polymer Degradation and Stability, 2011, V. 17, no. 61, pp. 507–514.

4. Bailey W. J., Kuruganli V.K., Angle J.S. Agriculture and synthetic polymers. Biodegradability and utilization. ACS symposium, 1990, V.2, pp. 149-160.

5. Markov A.V., Simonov-Emelyanov I.D., Prokopov N.I., Ganiev E.S., Anshin V.S., Markov V.A. research of technological properties of rigid PVC-compositions with various fillers. Vestnik MITIHT im. M.V. Lomonosov Moscow State University, 2012, N 4, pp. 100-105 (in Russ.).

6. Grigoryeva O., Fainleib A., Stepanenko L., Sergeeva L., Pissis P.Recycling of PVC/PU waste and reuse in PVC formulations: structure-property relationship. Polymer Engineering and Science, 2005, № 6, pp. 801-808.

7. Mallakpour S., Jarahiyan A., Iran J. An eco-friendly approach for the synthesis of biocompatible poly(vinyl alcohol) nanocomposite with aid of modified CuO nanoparticles with citric acid and vitamin C: mechanical, thermal and optical properties. Chemical Society, 2015, V. 3, no. 1, pp. 87-98.

8. Bazunova M.V., Prochukhan Y.A. Ways of utilization of polymers waste. Bulletin of the University of Bashkortostan, 2008, No. 4, pp. 875-885 (in Russ.).

9. Volkova K.V., Nosenko T.N., Uspenskaya M.V., Belukhichev E.V., Sivtsov E.V. Investigation of thermal characteristics of polymeric polymer composites based on polyvinyl chloride. Izvestiya SPbGTI (TU), 2017, T.40, no. 66, pp.55-60 (in Russ.).

10. Denisyuk I.Y., Pozdnyakova S.A., Koryakina I.G., Uspenskaya M.V., Volkova K.V. Polymer photodegradation initiated by ZnO nanoparticles. Optics and Spectroscopy, 2016, № 5, С. 778-781.

11. Lavrov N.A., Kolert K., Ksenofontov V.G., Lavrova T.V., Belukhichev E.V. On the Mechanism of Polyvinyl Chloride Degradation . Izvestiya SPbGTI (TU), 2012, no. 16 (42), pp. 31-35 (in Russ.).

**Biopolymer films based on chitosan and polyhydroxybutyrate**

**Glazacheva Ekaterina Nikolaevna**

ITMO University, PhD student.

Address: 197101, St. Petersburg, Kronverksky Pr., 49, Russia.

E-mail: termonna@mail.ru

+7 (812) 232-37-74

**Olekhnovich Roman Olegovich**

ITMO University, associate professor.

Address: 197101, St. Petersburg, Kronverksky Pr., 49, Russia.

E-mail: romanart@inbox.ru

+7 (812) 232-37-74

**Snetkov Petr Petrovich**

ITMO University, PhD student

Address: 197101, St. Petersburg, Kronverksky Pr., 49, Russia.

E-mail: ppsnetkov@corp.ifmo.ru

+7 (812) 232-37-74

**Uspenskaya Maya Valeryevna**

ITMO University, professor , The Head of the Chair of IT in the Fuel and Industry.

Address: 197101, St. Petersburg, Kronverksky Pr., 49, Russia.

E-mail: mv\_uspenskaya@mail.ru

+7 (812) 232-37-74

***Keywords:*** *chitosan, polyhydroxybutyrate, calcium chloride, biopolymer film.*

In this work, a nowel polymer film composition - chitosan/polyhydroxybutyrate/CaCl2 was prepared by solution-cast technique. The morphology of the surface and the structure of biopolymer films were studied by FTIR spectroscopy and optical microscopy. The effect of the concentration of calcium chloride from 0 to 15% on the structure and morphology of the surface of biopolymer films is demonstrated. The increase of CaCl2 content to 10 mass% leads to decrease of the surface heterogeneity of the films. Further increase in the content of calcium chloride provides the formation of network structure. The increase of elasticity of biopolymer films in 1.5 - 2 times with addition of calcium chloride to 10% is presented. The perspectives of materials based on polyhydroxybutyrate, chitosan and calcium chloride as film coatings for medical applications are shown.

**References**

1. Park S., Lih E., Park K., Jounga Y. K., Han D.K. Biopolymer-based functional composites for medical applications. Progress in Polymer Science, 2017, no. 68, pp.77-105.

2. Yunus Basha R., Sampath Kumar T.S., Doble M. Design of biocomposite materials for bone tissue regeneration. Materials Science & Engineering C, 2015, no. 57, pp.452-463.

3. Croisier F., Jerome C. Chitosan-based biomaterials for tissue engineering. European Polymer Journal, 2013, no. 49, pp.780-792.

4. Chernyshova E.B., Tuzhikov O.I., Nevestenko M.A., Berezin A.S., Yudin V.E., Dobrovol'skaya I.P. Study of modification of chitosan with low-molecular weight and polymeric aldehydes. Izvestia VSTU, 2015, no. 7, pp. 125-129 (in Russ.).

5. Ikejima T., Inoue Y. Crystallization behavior and environmental biodegradability of the blendfilms of poly(3-hydroxybutyric acid) with chitin and chitosan. Carbohydrate polymers, 2000, no. 41, pp.351-356.

6. Rennukka M., Amirul A.A. Fabrication of poly(3-hydroxybutyrate-co-4-hydroxybutyrate)/chitosan blend material: synergistic effects on physical, chemical, thermaland biological properties. Polymer Bulletin, 2013, no. 70, pp.1937-1957.

7. Bokeria L.A., Novikova S.P. Bioresorbable hydrogel polymer composition with biologically active substances (variants). RU 2519103, 2014. (in Russ.).

8. Pakhomov P.M., Khizhnyak S.D., Sitnikova V.E. IR spectroscopy for the analysis of scattering polymeric materials. Journal of Applied Spectroscopy, 2017, V. 84, no. 5, pp.837-842.

9. Onosova L.A., Kalinin A.A., Tseitlin G.M. Investigation of conformational transformations of macromolecules waterborne nitrogen-containing oligomers. Khimicheskaya promyshlennost’ segodnya [ Chemical Industry ], 2012, no. 6, pp. 32-35 (in Russ.).

10. Kann Y., Shurgalin M., Krishnaswamy R.K. FTIR spectroscopy for analysis of crystallinity of poly(3-hydroxybutyrate-co-4-hydroxybutyrate) polymers and it sutilization in evaluation of aging, orientation and composition. Polymer Testing, 2014, V. 40, pp.1-7.

11. Chen C., Zhou X., Zhuang Y., Dong L. Thermal Behavior and Intermolecular Interactions in Blends of Poly(3-hydroxybutyrate) and Maleated Poly(3-hydroxybutyrate) with Chitosan. Journal of Polymer Science Part B: Polymer Physics, 2005, V. 43, no. 1, pp.35-47.

**Effect of temperature on gel formation in sols of aluminosilicates and silicates**

**Khlebnikov Vadim** N.

Professor of the Department of physical and colloidal chemistry, Gubkin Russian State University of oil and gas (National Research University)

65 Leninsky Prospekt, Moscow, 119991, Russia

8499-507-86-93. E-mail: khlebnikov\_2011@mail.ru

**Rodnova Valentina** Y.

Engineer of the laboratory of materials and technologies for repair and insulation works in oil and gas wells LLC Scientific-Production Company Spetsburmaterially.1а Gastello str., Zhukovsky, Moscow region, 140180, Russia

8495-505-51-25, ext.4522. E-mail: valentinadinges@rambler.ru

**Hamidullina Inna** V.

Associate Professor at the Department of Industrial Safety and Industrial Ecology.

Ufa State Aviation Technical University, 450000, Ufa, K. Marks prosp., 12. Tel. (347) 2723633. E-­mail: inkaelf@mail.ru

***Keywords****: silicа sol, gelling kinetics, repair and insulation works.*

It was confirmed that in the acidic and alkaline regions of pH the time dependence of the gelation time of silica sols and aluminosilicates on temperature is satisfactorily described by an equation similar to the Arrhenius equation: **τ** = **τ**0 \* *exp*(*E*a/*RгT*). Arrhenius parameters of gel formation of acid sols of silica powder depend on the concentration of the activator and silica, and a relationship between the activation energy and the pre-exponential factor for acidic and alkaline silica sols is observed. In hydrochloric acid sols of aluminosilicates, the activation energy and pre-exponential gelling factors do not depend on the composition of the gel-forming solution.

**References**

1. Ralph K. Iler. The Chemistry of Silica. Solubility, Polymerization, Colloid and Surface Properties and Biochemistry of Silica. Part 1. Moscow, Mir Publ., 1982. 416 p. (in Russ.).

2. Ralph K. Iler. The Chemistry of Silica. Solubility, Polymerization, Colloid and Surface Properties and Biochemistry of Silica. Part 2. Moscow, Mir Publ., 1982. 717 p. (in Russ.).

3. Shabanova N. A. Sarkisov P. D. Fundamentals of sol-gel nanosized silica technology. Moscow, Akademkniga Publ., 2004. 208 p. (in Russ.).

4. Lozin E.V., Khlebnikov V.N. The use of colloidal reagents in oil production. Ufa, Bashnipineft' Publ., 2003. 236 p. (in Russ.).

5. Nozdrja V.I., Efimov N.N., Rodnova V.Ju., Hlebnikov V.N. Regularities gel formation of a concentrate silica sol in the presence of sodium salts. Bashkirskij himicheskij zhurnal [Bashkirskij Chemical Journal], 2016. no. 4. pp. 31-41.

6. Hangil'din G.N. Chemical plugging of wells. Moscow. Gostoptehizdat Publ. 1954. 123 p. (in Russ.).

7. M.Tsai. The study of formation colloidal silica via sodium silicate / Materials Science and Engineering B106 (2004), p. 52–55.

8. J.J. Jurinak, L.E.Summers, K.E.Bennet. SPE 18505 Supplement: Laboratory Testing of Colloidal Silica Gel for Oilfield Applications, SPE-23581-MS. J. SPE Prod. Eng, 1991.

9. Narottam P. Bansal. Influence of Several Metal Ions on the Gelation Activation Energy of Silicon Tetraethoxide. Journal of the American Ceramic Society. September 1990. Vol. 73, Is. 9. P. 2585–2778.

10. J. D. Hunt, S.M. Ezzedine, W. Bourcier, S. Roberts. Kinetics of the gelation of colloidal silica at geothermal conditions, and implications for reservoir modification and management. Thirty-Eighth Workshop on Geothermal Reservoir Engineering Stanford University, February 11-13, 2013 SGP-TR-198.

11. Komisarov A.I. Increasing the effectiveness of water inflow insulation in deep reservoirs // Trudy SevkazNIPIneft' [SevkazNIPIneft' Scientisic works]. 1990. V.52, pp. 34-39. (in Russ.).

12. L.K.Altunina. Composition for the isolation of high-permeability intervals of the formation. RU № 2094606 // St.2 –1997. -№30. – p.303. (in Russ.).

13. Hlebnikov V.N. Effect of concentration on gelling in sols of silicates and aluminosilicates / V.N. Hlebnikov, V.Ju. Rodnova, I.V. Hamidullina // Himicheskaja promyshlennost' segodnja [Chemical Industry Today]. № 6. - 2017. Pp. 21-28. (in Russ.).

14. Frolov Ju.G., Shabanova N.A., Popov V.V. Polycondensation of silicic acid in an aqueous medium. Influence of the concentration of silicic acid // Kolloid. Zhurnal [Colloid Journal]. 1983. V.45, №2. pp.382-386. (in Russ.).

15. Shabanova N.A., Kodinceva E.Ju. Influence of initial conditions on kinetics of gelling in hydrosols of silica // Kolloid. Zhurnal [Colloid Journal]. 1990. V.52, №3. pp. 553-558. (in Russ.).

16. Kontorovich S.I., Sokolova L.I., Ponomareva T.P. Influence of temperature on the kinetics of polycondensation of silicic acid // Kolloidnyj zhurnal [Colloid Journal]. 1984. V.46. №1. pp.127-130. (in Russ.).

17. Frolov Ju.G., Shabanova N.A., Savochkina T.V. Kinetics of gelling and spontaneous dispersion of silicic acid gel // Kolloid. Zhurnal [Colloid Journal]. 1980. V.42. №5. pp.1015-1018. (in Russ.).

18. Shabanova N.A. Kinetics of polycondensation in aqueous solutions of silicic acids // Kolloid. Zhurnal [Colloid Journal]. 1996. V.58, №1. pp.115-122. (in Russ.).

19. Frolov Ju.G., Shabanova N.A., Leskin V.V., Pavlov A.I. Preparation of stable silica powders // Kolloid. Zhurnal [Colloid Journal]. 1976. V.38, №6. pp.1205-1207. (in Russ.).

20. Denisov E.T. Kinetics of homogeneous chemical reactions. Moscow: Vysshaja shkola Publ., 1988. 392 p. (in Russ.).

21. C. Dixit, M. Bernard, B. Sanjuan, L. André, S. Gaspard. Experimental study on the kinetics of silica polymerization during cooling of the Bouillante geothermal fluid (Guadeloupe, French West Indies) / Chemical Geology. - 2016. - V. 442. - Р. 97-112.

22. Hamouda, A.A. Factors Affecting Alkaline Sodium Silicate Gelation for In-Depth Reservoir Profile Modification / А.А. Hamouda, Н.А. Amiri // Energies. - 2014. - V. 7. - Р. 568-590.

**Optimization of the process for the preparation of sodium isobutylate**

**Semin Alexey Viktorovich**

State Scientific Research Institute of Organic Chemistry and Technology, Senior Researcher. 111024, Moscow, sh. Enthusiasts, 23.

**Kazakov Pavel** Vasilyevich

State Scientific Research Institute of Organic Chemistry and Technology, Doctor of Chemical Sciences, Head of the Department of Technological Development.111024, Moscow, sh. Enthusiasts, 23. E-mail: dir@gosniiokht.ru

**Gorelenko Svetlana** Vasilyevna

State Scientific Research Institute of Organic Chemistry and Technology, Candidate of Technical Sciences, Senior Researcher.111024, Moscow, sh. Enthusiasts, 23.

**Mirzabekova Natalya** Sergeevna

State Scientific Research Institute of Organic Chemistry and Technology, Doctor of Chemical Sciences, Leading Researcher.

111024, Moscow, sh. Enthusiasts, 23. E-mail: dir@gosniiokht.ru

***Keywords:*** *sodium isobutylate, sodium hydroxide, aromatic hydrocarbons****.***

A method for the synthesis of sodium isobutylate from an aqueous solution of sodium hydroxide and isobutyl alcohol in the presence of aromatic hydrocarbons suitable for use in industrial conditions is proposed. The use of aromatic hydrocarbons in the production of alcoholates increases the intensity of the process and contributes to a more complete separation of water upon stratification of the heteroazeotrope. Partial replacement of isobutanol with an aromatic hydrocarbon increases the solubility of the alcoholate in the mixed solvent, which allows one to obtain concentrated solutions that do not crystallize at room temperature, which greatly extends their use in organic synthesis. The data obtained can be used both in laboratory practice and in the production of sodium isobutylate in the industrial version.

**References**

1. Patent WO2013168113 C07C29/70; C07C31/30 Metod for preparing alkali metal alkoxides. Abadias H. Carlevaris R. Horowitz G. et al., 2013.

2. Patent DE 968903 C07C29/70; C07C31/30. Verfahren zur kontinuierlichen Herstellung von Alkalialkoholaten. Coenen DR Alfred, 1958.

3. Gjaldbaek J.C. On the reaction carbon monoxide and alcohole catalyzed by alcoholate. Acta Chem. Scand., 1948, 2, p. 687.

4. Patent GB 377631 C07C29/70. Manufacture of alkali alcoholates. Wacker Chemie GMBH, 1932.

5. Patent US 1910331 C07C29/70. Process of preparing alkali metal aliphatic monohydroxy alcoholates. Halbig P., 1933.

6. Дыханов Н.Н, Скрипкина В.Т. Методы получения химических реактивов и препаратов. М., ИРЕА, 1964, №9, с. 28-29.

7. А.с. СССР №198316. МПК С07с. Способ получения бутилата калия и натрия. Воробьева В.Я., Городецкий Л. Ш., Зейфман В. И. и др.,Бюлл. № 14, 1962.

8. А.с. СССР № 202102. МПК С07с. Миропольская М.А., Егорова В.В., Валашек И.Е., Самохвалов Г.И. Способ получения 9-метил-7-(1.1.5-триметилциклогексен-5-ил)-бутен-8-аля-10 (альдегида β-С14), Бюлл. №19, 1967.

9. А.с. СССР № 639848. МПК C07C31 / 30 Способ получения изобутилата калия. Савченко Г.Б., Золотарев Н.С., Бельченко И.И., Бюлл.№ 48, 1978.

10. Рабинович В.А., Хавин З.Я. Краткий химический справочник. «Химия», Л., 1978 г., стр. 259.

References:

1. Abadias H. Carlevaris R. Horowitz G. et al. Method for preparing alkali metal alkoxides. WO 2013168113, 2013.

2. Coenen DR. Alfred. Verfahren zur kontinuierlichen Herstellung von Alkalialkoholaten. DE 968903, 1958.

3. Gjaldbaek J.C. On the reaction carbon monoxide and alcohole catalyzed by alcoholate. Acta Chem. Scand., 1948, no 2, p. 687.

4. Wacker Chemie GMBH. Manufacture of alkali alcoholates. GB 377631, 1932.

5. Halbig P. Process of preparing alkali metal aliphatic monohydroxy alcoholates. US 1910331, 1933.

6. Dykhanov NN, Skripkina V.T. Methods of obtaining chemical reagents and preparations. М., IREA, 1964, no 9, pp 28-29. (in Russ.).

7. Vorob'eva V.Ya., Gorodetsky L.Sh., Zeifman V.I. and ol. Method for the preparation of potassium and sodium butoxide. A.s. USSR 198316, 1962. (in Russ.).

8. Miropolskaya M A, Egorova V V, Valasek IE, Samokhvalov G I. Method for the preparation of 9-methyl-7-(1.1.5-trimethylcyclohexen-5-yl)-butene-8-ala-10 (aldehyde β-C14). A.s. USSR 202102, 1967. (in Russ.).

9. Savchenko G B, Zolotarev N S, Belchenko I I. Method of obtaining potassium isobutylate. A.s. USSR 639848, 1978. (in Russ.).

10Rabinovich V A, Khavin Z.Ya. Brief Chemical Handbook. «Chemistry», L, 1978, p 259 (in Russ.).

**Indicators of energy efficiency of mass transfer columns with random packings**

**Laptev Anatoliy** Grigorievich

“Kazan State Power Engineering University”

Аddress: 420066, Kazan, st. Krasnoselskaya d.51

Tel.rab: (843) 519-42-54. Tel: 8-9050-20-85-33. E-mail: tvt\_kgeu@mail.ru

**Basharov Marat** Minnahmatovich

JSC "TANECO".

Аddress: 423570 , Nizhnekamsk, 97 RUPS. E-mail: taneco.basharov@gmail.ru

Tel.: (8555) 49-02-02

***Keywords****: mass transfer, random packing, energy efficiency, pressure drop.*

Various expressions for estimating the mass transfer and hydraulic efficiency of packed columns are considered for the cases, in which the main resistance to mass transfer is concentrated in the gas phase (evaporation and absorption processes). Complexes developed by Sokolov V.N., Domansky I.V. as well as energy coefficient by Spalding D.B were used. An expression for calculating a criterion for energy efficiency of a mass transfer process for a packed column was obtained, in which the main parameters are the Murphree mass transfer efficiency, pressure drop and working volume of the apparatus.Results of calculations of the pressure drop and the efficiency criterion for packings having the same specific surface area are shown, which include Raschig and Pall rings, as well as GIAP-NZ and Inzhekhim-2000. Similar calculations were made using the Spalding coefficient. Qualitative agreement of calculation results was noted. Conclusions are drawn about the most energy efficient designs and operating modes of packed columns.

**References**

1. Ostrovsky G.M., Ziyatdinov N.N., Lapteva T.V. Optimization of technological systems. M.: KNORUS, 2012. 424 p. (in Russ.).

2. Gortyshov Yu.F., Olimpiev V.V., Baigaliev B.E. Thermohydraulic calculation and design of equipment with intensified heat transfer. Kazan: Kazan A.N. Tupolev State Technical University Press, 2004. 432 p. (in Russ.).

3. Dzyubenko B.V., Kuzma-Kichta Yu.A., Kutepov A.M. et al. Intensification of heat and mass transfer in power engineering. M.: FGUP “TsNIIAtom-inform”, 2003. 232 p. (in Russ.).

4. Laptev A.G., Basharov M.M. Efficiency of heat and mass transfer and separation of heterogeneous media in apparatuses of the oil and gas chemical complex. Kazan: Center for innovation technologies, 2016. 344 p. (in Russ.).

5. Sokolov V.N., Domanskii I.V. Gas-liquid reactors. Leningrad: Mashinostroenie, 1976. 216 p. (in Russ.).

6. Ramm V.M. Absorption of gases. M.: Khimiya Publishing House, 1976. 656 p. (in Russ.).

7. Aleksandrov I.A. Mass transfer in distillation and absorption of multicomponent mixtures. Leningrad: Khimiya Publishing House, 1975. 319 p. (in Russ.).

8. Laptev A.G., Lapteva E.A. Determination of the coefficients of turbulent mixing in one- and two-phase media by Taylor model. Fundamentalnie issledovaniya [Fundamental research], 2015, no.2, pp. 2810-2814 (in Russ.).

9. Laptev A.G., Farakhov T.M., Lapteva E.A. Models of transport phenomena in random packed and granular beds. Teoreticheskie osnovi himicheskoy tehnologii [Theoretical foundations of chemical engineering], 2015, v.49, no.4, pp. 388–395 (in Russ.).

10. Sokol B.A., Chernyshev A.K., Baranov D.A. Packings of mass transfer columns. M.: Galleya-print, 2009. 358 p. (in Russ.).

11. Kagan A.M., Laptev A.G., Pushnov A.S., Farakhov M.I. Contact packings of industrial heat and mass transfer apparatuses. Kazan: Otechestvo, 2013. 454 p. (in Russ.).

**On the possibility of domestic engineering to provide processing and environmental equipment production for the implementation of BAT**

**Muratov Evgenij Vladislavovich**

The Ministry of industry and trade of the Russian Federation, Deputy Director of the Department of machine and investment engineering

Tel. + 7 (495) 647-74-74

Email: muratov@minprom.gov.ru

**Troshchenkov Ivan Olegovich**

The Ministry of industry and trade of the Russian Federation, Deputy Head of Department of development of mining and heavy engineering, Department of mechanical engineering and machine tool industry

Tel. +7 (495) 632-88-88, ext. 1970.

E-mail: Troschenkov@minprom.gov.ru

**Kostyleva Vera Mihajlovna**

Federal State Autonomous Body Research Institute «Environmental Industry Policy Centre», Chief of Department of Chemical and Petrochemical Industry.

141006, Moscow Region, Mytishchi, Olimpijskij prospect, 42

+7 (495) 240-00-00 (ext. 1100)

v.kostyleva@eipc.center

**Malyavin Andrej Stanislavovich**

Federal State Autonomous Body Research Institute «Environmental Industry Policy Centre»,

Deputy Chief of Department of Chemical and Petrochemical Industry.

141006, Moscow Region, Mytishchi, Olimpijskij prospect, 42.

+7 (495) 240-00-00 (ext. 1101). E-mail: a.malyavin@eipc.center

**Popov Aleksandr Yur'evich**

Federal State Autonomous Body Research Institute «Environmental Industry Policy Centre», Senior Researcher of Department of Chemical and Petrochemical Industry. 141006, Moscow Region, Mytishchi, Olimpijskij prospect, 42.

+7 (495) 240-00-00 (ext. 1104). E-mail: a.popov@eipc.center

***Keywords:*** [*Best Available Technique*](https://www.multitran.ru/c/m.exe?t=7589607_1_2)*s, basic process equipment, environmental protection equipment, government support.*

The status of the basic process equipment manufacturing operated in case of application of the [Best Available Technique](https://www.multitran.ru/c/m.exe?t=7589607_1_2)s is characterized. The domestic engineering production incentives are described. The BAT equipment is sorted by type and purpose in the context of equipment list related to the application area of the Reference Document on Best Available Techniques in the «Ammonia, Fertilizers and Inorganic Acids production». The possibility of BAT equipment manufacturing in the Russian Federation is estimated as well as recommendations for government support of equipment manufacturers are given. Equipment manufacturers from a group which includes gas cleaning equipment, heat exchange equipment, compressors and superchargers and some other devices, can be considered as potential subjects of state support for its cost-effective production, including within the framework of import substitution programs.

**References**

1. Executive Order On National Goals and Strategic Objectives of the Russian Federation through to 2024, May 7, 2018 ( in Russ).

2. Federal Law of 21 July 2014 No. 219-FZ "On Amending the Federal Law on Environmental Protection"( in Russ).

3. Guseva T.V., Molchanova Y.P., Begak M.V., Mironov A.V. Best available technologies as an instrument of industrial and environmental policy // Vestnik rossijskogo himiko-tekhnologicheskogo universiteta imeni D. I. Mendeleeva: gumanitarnye i social'no-ehkonomicheskie issledovaniya [Bulletin of the D. Mendeleev University of Chemical Technology of Russia: humanitarian and socio-economic research], 2015, Vol. 2, No. 6, P. 62-76 ( in Russ).

4. Federal Law of December 31, 2014 No. 488-FZ "On Industrial Policy in the Russian Federation" (in Russ).

5. Federal Law of 10 January 2002 No. 7-FZ "On Environmental Protection" ( in Russ).

6. Resolution of the Russian Government of June 20, 2017 No. 1299-r( in Russ).

7. Resolution of the Russian Government of April 7, 2018 No. 622-r( in Russ).

8. Resolution of the Russian Government of March 19, 2014 No. 398-r ( in Russ).

9. Resolution of the Russian Government of December 24, 2014 No. 2674-r ( in Russ).

10. Order of the Russian Government of 30.12.2013 No. 1312 ( in Russ).

11. Order of the Russian Government of 03.01.2014 No. 3 ( in Russ).

12. Order of the Russian Government of 10.10.2014 No. 1044 ( in Russ).

13. Order of the Russian Government of 12.03.2015 No. 214 ( in Russ).

14. Order of the Russian Government of 17.07.2015 No. 719 ( in Russ).

15. Order of the Russian Government of 04.08.2015 No. 785 ( in Russ).

16. Resolution of the Russian Government of 29.12.2015 No. 2744-r ( in Russ).

17. Resolution of the Russian Government of 31.12.2015 No. 2781-r ( in Russ).

18. Order of the Ministry of Industry and Trade of the Russian Federation of March 31, 2015 No. 645 ( in Russ).

19. Order of the Ministry of Industry and Trade of the Russian Federation of March 31, 2015 No. 653 ( in Russ).

20. Order of the Ministry of Industry and Trade of the Russian Federation of March 31, 2015 No. 654 ( in Russ).

**Removal of heavy metals from mining wastewater**

**Kagramanov George** Gaikovich

D.Tech.Sc., Professor, Head of Department of Membrane Technology

D.Mendeleev University of Chemical Technology of Russia

125047, 9 Miusskaya sq., Moscow, Russian Federation

Tel: +7 499 978 82 60.

E-mial: kadri@muctr.ru

**Farnosova Elena** Nikolaevna

Ph.D, Associate Professor, Department of Membrane Technology

D.Mendeleev University of Chemical Technology of Russia

125047, 9 Miusskaya sq., Moscow, Russian Federation.

Tel: +7 499 978 82 60.

E-mial: farelena@rambler.ru

**Lin Maung Maung**

Post graduate student, Department of Membrane Technology

D.Mendeleev University of Chemical Technology of Russia

125047, 9 Miusskaya sq., Moscow, Russian Federation.

E-mail: linmg51@gmail.com

**Blanco-Pedrekhon Alexandra** Maksimovna

Master student, Department of Membrane Technology

D.Mendeleev University of Chemical Technology of Russia

125047, 9 Miusskaya sq., Moscow, Russian Federation.

E-mial: aleksandra94@list.ru

***Keywords:*** *ultrafiltration, nanofiltration, reverse osmosis, mining wastewater, heavy metals.*

Pressure driven membrane processes, such as reverse osmosis (RO), nanofiltration (NF) and ultrafiltration (UF) are widely used in water purification and various wastewater treatment systems. Ultrafiltration is suitable for pre-treatment of nanofiltration and reverse osmosis systems. The main characteristics of nanofiltration and reverse osmosis membranes (flux and rejection) in purification of wastewaters containing manganese ions were studied. The influences of main technological parameters: feed solution concentration and pH value, on flux and rejection of NF and RO membranes are considered. The minimum rejection point (isoelectric point) of NF membrane in purification of wastewaters (including mining ones) from manganese ion has been determined.

**References**

1. Frog B.N., Pervov A.G. Vodopodgotovka // Uchebnikdlyavuzov. — M.: Izdatel'stvo АСВ, 2015. — 512 p. (in Russ.).

2. Lin Maung Maung, Farnosova E.N., Kagramanov G.G. Heavy metals containing wastewater purification by nanofiltration and ion exchange methods // (Chemical Industry Today). 2017. № 8. pp 30 – 35. (in Russ.).

3. S. Shaaban., H. Yahya. Detailed analysis of reverse osmosis systems in hot climate conditions // Desalination, 2017, vol. 423, pp 41 – 51.

4. Timothy V. Bartholomew., Laura Mey., Jason T. Arena., Nicholas S. Siefert., Meagan S. Mauter. Osmotically assisted reverse osmosis for high salinity brine treatment // Desalination, 2017, vol. 421, pp 3 – 11.

5. Paz Nativ., OriLahav., YouriGendel. Separation of divalent and monovalent ions using flow-electrode capacitive deionization with nanofiltration membranes // Desalination, 2018, vol. 425, pp 123 – 129.

6. Julio Lopez., Monica Reig., AndriyYaroshchuk., EdxonLicon., OriolGibert., Jose Luis Cortina. Experimental and theoretical study of nanofiltration of weak electrolytes: SO42-/HSO4-/H+ system // Journal of Membrane Science, 2018, vol. 550, pp 389 – 398.

7. Miriam C.S. Amaral., Luiza B. Grossi., Ramatisa L. Ramos., Barbara C. Ricci., Laura H. Andrade. Integrated UF-NF-RO for gold mining effluent treatment: From bench-scale to pilot-scale // Desalination, 2018, vol. 432, pp 120 – 128.

8. Saren Qi., Wangxi Fang., WinnaSiti., WentaliaWidjajanti., Xiao Hu., Rong Wang. Polymersomes-based high-performance reverse osmosis membrane for desalination // Journal of Membrane Science, 2018, vol. 555, pp 177 – 184.

9. Ditnerski Y.I. Reverse Osmosis and Ultrafiltration // М.: Chemiya, 1978. – 352 p. (in Russ.).

10. Saren Qi., Wangxi Fang., WinnaSiti., WentaliaWidjajanti., Xiao Hu., Rong Wang. Polymersomes-based high-performance reverse osmosis membrane for desalination // Journal of Membrane Science, 2018, vol. 555, pp 177 – 184.

11. GOST R 52407-2005., Drinking water. Methods for determining of hardness. M: The national standard of the Russian Federation, 2007. (in Russ.).

12. Loiko A.V., Shibanov I.V., Kagramanov G.G., Blanco-Pedrekhon A.M. Experience in the introduction of membrane technology for cleaning artesian waters with a high content of iron and manganese // Water Purification, Water Preparation, Water Supply, 2018 № 4, pp 58-62. (in Russ.).

13. J.J. Qin., M.H. Oo., H. Lee., B. Coniglio. Effect of feed pH on permeate pH and ion rejection under acidic conditions in NF process // Journal of Membrane Science, 2004, vol. 232, pp 153 – 159.