**Synthesis of nanofibrous carbon on catalysts, prepared by solution combustion technique**

**Kurmashov Pavel B.,** Novosibirsk State Technical University, engineer, е-mail: [kurmaschov@gmail.com](mailto:kurmaschov@gmail.com)

**Bannov Alexandr G.,** Novosibirsk State Technical University, PhD, docent, е-mail: bannov\_a@mail.ru

**Dyukova Kseneya D,** Novosibirsk State Technical University, engineer, е-mail: dyukova\_kx701@mail.ru

**Netskina Olga V.,** Boreskov Institute of Catalysis, PhD, researcher, е-mail: netskina@catalysis.ru

**Ukhina Arina V**, Institute of Solid State Chemistry and Mechanochemistry, engineer, е-mail: [root@solid.nsc.ru](mailto:root@solid.nsc.ru)

**Kuvshinov Gennagiy G.**, Sochi State University, Doctor of Sсience, professor, е-mail: [gennady.kuvshinov@gmail.com](mailto:gennady.kuvshinov@gmail.com) наука

**Keywords**: catalyst, solution combustion, catalytic pyrolysis, nanofibrous carbon, specific yield

**Abstract**. The catalysts for decomposition of methane to carbon nanofibers and hydrogen were prepared by solution combustion method. By using optical and scanning electron microscopy was studied morphology of the obtained samples. Samples containing 90 wt.% nickel and 10 wt. % aluminum oxide were tested in the decomposition of methane at a temperature of 550 ° C and 1 atm. Experimental studies of the catalysts were carried out in a quartz flow reactor. It was shown that structural, textural and catalytic properties of the catalysts depend on features of their preparation. The optimal parameters of the catalyst preparation, that provide high specific yield of the carbon nanofibers and hydrogen until the catalyst deactivation, were established.

**References**

1. Hughes T.V. and Chembers C.R., US Patent No. 405480, 1889.

2. Radushkevich L.V., Lukyanovich V.M. O structure ugleroda, obrazuyushchegosya pri termicheskom razlozhenii oksida ugleroda na zheleznom kontakte. Zhurnal fizicheskoj khimii, 1952, vol 25, issue 1, pp.87.

3. Jong K.P., Geus J.W. Carbon nanofibers: catalytic synthesis. Catal. Rev.-Sci. Eng. 2000;42(4), 481–510.

4. Kuvshinov G.G. Environmentally sound nontraditional processing of hydrocarbon energy carriers to produce and use hydrogen. // Proc. of The Third Int. Conf. on New Energy Systems and Conversions, September, 8-13, 1997, Kazan, Russia.

5. Kuvshinov G.G., Parmon V.N., Sadykov V.A., Sobyanin V.A. New catalysts and catalytic processes to produce hydrogen and syngas from natural gas and other light hydrocarbons. // Studies in Surface Science and Catalysis, 1998, Vol. 119. p. 677.

6. Rodriguez N.M. A review of catalytically grown carbon nanoribers. J. Mater. Res. 1993; 8(12):3233.

7. Kuvshinov G.G., Chukanov I.S., Krutsky Y.L., Ochkov V.V., Zaikovskii V.I., Kuvshinov D.G..Changes in the properties of ﬁbrous nanocarbons during high temperature heat treatment. Carbon 47 (2009) 215-225.

8. Kuvshinov G.G., Zavaruchin S.G., Mogil’nykh Yu.I., Kuvshinov D.G. Realizatsija protsessa polucheniya granulirovannogo kataliticheskogo voloknistogo ugleroda v mashtabe pilotnogo reaktora. Khimicheskaja promyshlennost, 1998, issue 5, pp.300-307.

9. Michakov I.V., Buyanov R.A., Chesnokov V.V., Strel’tsov I.A., Vedjagin A.A. Technologiya polucheniya uglerodnych nanorazmernykh nitey po mechanizmu karbidnogo tsikla. Kataliz v promyshlennosti, 2008, issue 2, pp. 26-31.

10. Kuvshinov G.G., Mogilnykh Yu.I., Kuvshinov D.G., Ermakov D.Yu., Ermakova M.A., Salanov N.A., Rudina N.A. Mechanism of porous filamentous carbon granule formation on catalytic hydrocarbon decomposition. // Carbon 37, (1999), p. 1239 – 1246.

11. Fenelonov V.B., Avdeeva K.B., Zheyvot V.I., Okkel’ L.G., Goncharova O.V, Pimneva L.G. Tekstura i adsorbtsionnye svoystva voloknistogo ugleroda, poluchaemogo razlozheniem uglerodsoderzhashchih gazov na metallicheskich katalizatorov. Kinetika i kataliz, 1993, vol 34, issue 3, pp.545-549.

12. Shinkarev V.V., Glushenkov A.M., Kuvshinov D.G. and Kuvshinov G.G.. Nanofibrous carbon with herringbone structure as an effective catalyst of the H2S selective oxidation. // Carbon. - 2010. –V. 48. –P. 2004–2012.

13. Asedegbega-Nieto E., Bachiller-Baeza B., Kuvshinov D.G., García-García F.R., Chukanov E., Kuvshinov G.G., Guerrero-Ruiz A., Rodríguez-Ramos I. Effect of the carbon support nano-structures on the performance of Ru catalysts in the hydrogenation of paracetamol. // Carbon, 46, Issue 7, June 2008, 1046-1052.

14. Kovalenko G.A., Kuznetsova E.V., Mogilnykh Yu.I., Andreeva I.S., Kuvshinov D.G., Rudina N.A. Catalytic filamentous carbons for immobilization of biologically active substances and non-growing bacterial cells. // Carbon 39 (2001) 1033–1043.

15. Hammel E., Tang X., Trampert M., Schmitt T., Mauthner K., Eder A., Potschke P. Carbon nanoﬁbers for composite applications. // Carbon 42 (2004) 1153–1158.

16 Bannov A.G., Uvarov N.F., Shilovskaya S.M., Kuvshinov G.G. Effect of the preparation methods on electrical properties of epoxy resin // Carbon nanofiber composites. // Nanotechnologies in Russia. – 2012. – V. 7(3–4) –P. 169–177.

17. Pham-Huu C., Keller N., Ehret G., Ledoux M.J. The first preparation of Silicon Carbide Nanotubules by Shape Memory Synthesis and Their Catalytic Potential. Journal of Catalysis, 200 (2001) 400-410.

18. Tomishko M.M., Demicheva O.V., Alekseev A.M., et. al. Mnogoslojjnye uglerodnye nanotrubki i ikh primenenie. Rossijjskijj khimicheskijj zhurnal, 2008, vol 52, issue 5, pp.39-43.

19. Patent RF 2064831. Sposob polucheniya vodoroda i uglerodnogo materiala. [АНГЛ]. Avdeeva L.B., Goncharova O.V., Kuvshinov G.G., Likholobov V.A., Parmon V.N. Declared 01.03.1994. Published 10.08.1996. Bulletin No. 22. (In Russian).

20. Molchanov V.V., Buyanov R.A. Mekhanokhimiya katalizatorov. Uspekhi khimii, 2000, vol 69, issue 5, pp.476-493.

21. Patent RF 2126718. Sposob prigotovleniya katalizatorov.. Ermakov D.Yu., Ermakova M.A., Kuvshinov G.G. Declared 1999. Published 12.03.1997. (In Russian).

22. Ermakova M.A., Ermakov D.Yu., Kuvshinov G.G., Plyasova L.M. New Nickel Catalysts for the Formation of Filamentous Carbon in the Reaction of Methane Decomposition. // J. Catal., 187 (1999), p. 77-84

23. Rosl’yakov S.I., Kovalev D. Yu., Rogachov A.S., Manukjan Kh., Mukas’yan A.S. Gorenie rastvorov: dinamika fazoobrazovaniya pri sinteze vysokoporistogo nikelya. Doklady akademii nauk, 2013, vol 449, issue 3, pp.313.

24. Prakash A.S., Khadar A.M.A., Patil K.C., and Hegde M.S., Hexamethylenetetramine: A New Fuel for Solution Combustion Synthesis of Complex Metal Oxides. // Journal of Materials Synthesis and Processing, vol. 10, pp. 135-141, May 2002.

25. Tkachev A.G. Opredelenie sostava i metoda polucheniya katalizatorov sinteza uglerodnych nanostrukturnykh materialov, Tambov, 2007, vol 2, issue 4, pp.166-174.

26. Adler Yu.P., Markova E.V., Granovskiy Yu.V. Planirovanie eksperementa pri poiske optimalnykh usloviy. Moskva, 1976, pp.279.

**The conversion of linear hydrocarbons on the zeolite catalyst**

**Narenkov Roman** Y, post graduate student D.Mendeleyev University of Chemical Technology of Russia, e-mail: [nar-roman@rambler.ru](mailto:nar-roman@rambler.ru)

**Kladova Darya Y**., master D. Mendeleyev University of Chemical Technology of Russia, e-mail: kladych@mail.ru

**Sapunov Valentin** N., professor D.Mendeleyev University of Chemical Technology of Russia, e-mail: sapunovvals@gmail.com

**Keywords:** paraffins, olefins, catalysis, cracking, resin, methane, polyaromatic compounds

**Abstract:** The process of catalytic cracking some paraffin’s and olefins produced in processing of methanol, such as MTO (methanol-to-olefin) and MTG (methanol-to-gasoline) was investigated. As the catalyst was used for such processes typical zeolite НВКЦ (high-silica zealots in the H form) + 0,5% P2O5 based on ZSM-5 (Si / Al = 220), which showed high activity in the conversion of linear hydrocarbons in the gaseous and liquid products. In the gaseous reaction products dominated mostly lower olefins. In the liquid products were determined cyclic and aromatic hydrocarbons and compounds which are formed from olefins, but they were not detected. The amount of olefins and aromatic hydrocarbons liquid products increases with contact time or reaction temperature. It was established that the rate of conversion pairs olefin/paraffin’s (octane / octene and nonane / nonene) are approximately equal. Identified the main regularities of can extend the resource base to produce products of basic organic synthesis.

**References**

1. Tanabe K., Holderich W.F., Appl. Catal. A:General 1999, 181, 399.

2. Chang C.D., Silvestri A.J., J. Catal., 1977, 47 (2), 249.

3. Olah G.A., Doggweiler H., Felberg J.D. et al., J. Amer. Chem. Soc., 1984, 106 (7), 2143.

4. Hutchings G.J., Johnston P., Lee D.F. et al., J. Catal., 1994, 147 (1), 177.

5. Gordon A., Ford R. Sputnik khimika. M., Mir, 1976, s.437.

6. Narenkov R.Yu., Kladova D.Yu., Sapunov V.N. Kataliz modifitsirovannymi tseolitami protsessa konversii metanola v uglevodorody// Khimicheskaya promyshlennost' segodnya 3 (2014) str. 11–19.

7. Patent RF № 2487160. Sposob kataliticheskogo krekinga uglevodorodnogo syr'ya s vysokim vykhodom legkikh olefinov i ustroystvo dlya ego osushchestvleniya. Solyar Boris Zakharovich (RU), Glazov Leonid Shaevich (RU), Mnev Maksim Vladimirovich (RU), Klimtseva Elena Ar'evna (RU). 26.03.2012.

8. A P. V. Lipin, V. P. Doronin, and T. I. Gulyaeva. Conversion of Higher n%Alkanes under Deep Catalytis Cracking Conditions// Petroleum Chemistry, 2010, Vol. 50, No. 5, pp. 362–367.

9. Hiroki Konno, Takuya Okamura, Takahito Kawahara, Yuta Nakasaka, Teruoki Tago, Takao Masuda. Kinetics of n%Hexane Cracking over ZSM%5 Zeolites Effect of Crystal Size on Effectiveness Factor and Catalyst Lifetime//Chemical Engineering Journal (2012).

10. Dumskiy, Yu. V. Khimiya i tekhnologiya neftepolimernykh smol: monografiya // Yu. V. Dumskiy, B. I. No, G. M. Butov. — M.: Khimiya, 1999.% 312 s.

11. E.G. Rakov: «Nanotrubki i fullereny», M.: Universitetskaya kniga, Logos. 2006. – 376 s.

**Phosphorus extraction from a ferrophosphorus with a ferrosilicon**

**Serzhanov Galimzhan** M. Master of Technical Sciences, doctoral candidate, South Kazakhstan State University named after M. Auezov, Shymkent, Tauke khan avenue, 5, 160012, Kazakhstan; e-mail: [gsm\_ask@mail.ru](mailto:gsm_ask@mail.ru)

**Shevko Viktor** M. – Doctor of Technical Sciences, professor, South Kazakhstan State University named after M. Auezov, Shymkent, Tauke khan avenue, 5, 160012, Kazakhstan; e-mail: [v\_shevko@mail.ru](mailto:v_shevko@mail.ru),

**Lavrov Boris** A. Doctor of Technical Sciences, professor, St. Petersburg State Technological Institute (Technological University), St. Petersburg, Moscow avenue, 26, 190013, Russia; e-mail: [ba\_lavrov@mail.ru](mailto:ba_lavrov@mail.ru)

**Keywords:** ferrophosphorus, iron phosphides, calcium silicides, thermodynamics, balance, ferrosilicium, phosphorus.

**Abstract**. This article contains the research results of the determination of optimum parameters of the phosphorus extraction from a ferrophosphorus produced by the limited partnership “Kazphosphate” with a phosphorus content 20,4 % and 26,2 % with the using the second degree rotostandard plan. The adequate equations of regression, time effect, temperature effect and influence of a ferrosilicon (FS65 grade)-ferrophosphorus ratio on a phosphorus extraction degree in a gas phase were received. It was found, that 85-88 % of phosphorus is extracted from theferrophosphorus, containing 20,4 % of phosphorus, at 1780-18000C, the process duration 104-120 minutes and the FS65 /ferrophosphorus ratio in the initial charge 3,0; and from the ferrophosphorus containing 26,2 % of phosphorus – at 1790-18000C, the process duration 109-120 minutes and the FS65/ferrophosphorus ratio2,4.

**References**

1. Ershov V.A., Pimenov S.D. Electrotermia phosphora.-SPb:Himia, 1996.-248s.
2. Konevskiy M.R. Ferrophosphor kak legiruyuschiy splav I osnova dlja novih sposobov poluchenija himicheskoj i metallurgicheskoj produkciy// Sbornik trudov Vserossijskoj nauchno-tehnicheskoj konferenciy «Electrotermia-2010» - S-Peterburg.-2010.-s. 39-44.
3. ST TOO 390838120141-005-2010.Ferrophosphor electrotermicheskij. Tehnicheskie uslovija. TOO Kazfosfat. 2010g.-22 s.
4. Ershov V.A. Ferrosplavi v himicheskoi promishlennosti. L.:LTI-1980.-70s.
5. Metodi pererabotki ferrophosphora / Obzor pod redakciej Teterevkova A.I., Fominoi E.A., Shubaeva V.L. L.: NIETHIM. – 1973.-30s.
6. Protopopov F.V. Nauchnie osnovi i tehnologii metallurgicheskoj pererabotki ferrophosphora v specialnie materiaki i izdelija. Avtoreferat dis. dokt. tehn.nauk. Almati.2002-35 s.
7. Pat. № 2373142(13) RF. Sposob obrabotki rasplava ferrophosphora / Genkin M.V., Shvecov S.V.; opubl. 20.11.2009.
8. Tlebaev M.B., Ualieva Z.U., Kazova A.M. Termodinamicheskij analiz i modelirovanie processa obziga splava phosphidov zeleza //Vestnik VKGTU imeni D. Serikbaeva.-Ust-Kamenogorsk, 2008.-№3.-S.49-53.
9. A.S. 209472126 SSSR. Sposob pererabotki ferrophosphora na phosphoristie shlaki// Konevskij M.R., Hodakova E.A.; opubl. 30.04.76.,Bul. №16.
10. <http://en.wikipedia.org/wiki/Phosphorus_pentasulfide>
11. Pат. СN1884052, C01B25/18, С01В 25/00. Opubl. 27.12.2006
12. Pат.US 4014682, C21B 3/04, C21B 13/00. Opubl. 29.03.1977
13. Pат. RU 2373142, C01B 25/08. Opubl. 20.11.2011.
14. Kunaev A.M., SWuharnikov U.I., i dr. issledovanie processa vakuumtermicheskoi pererabotki ferrophosphora// Trudi IMiO ANKazSSR. 1972. TXLIV(44), S.30-34.
15. Bills P.M., Hoyle G., Lowe E.J., Pат. Anglii, 971343, zajavlen. 21.12. 1961, opubl. 30. 09. 1963. Pат. Francii, 1. 342. 555, zajavlen. 21. 12. 1962. opubl. 30.09.1963.
16. Gall J. F., Barth-Wehrenalp G., Pат USA, 2838372, zajavlen. 05. 07. 1955, opubl. 10. 06. 1958.
17. Ragulina R.I., Emlin B.I. Electrotermia kremnija i silumina. M.:Metallurgija. 1992.-240 s.
18. Ljakishev N.P., Gasik M.I., Dashevskij V.J. Metallurgija ferrosplavov. Chast 1.-M.:MiSiS, 2006.-117 s.
19. RoineA.Outokumpu HSС Chemistry for Windows. Chemical Reaction and Eguilibriumloftware with Extensive Thermochemical Database.Pori:Outokumpu Research OY,2002
20. Ahnazarova S.L., Kafarov V.V. Metodi optimizacii experimenta v himicheakoj promishlennosti. M.: Visshaja shkola, 1978.-319 s.
21. Ochkov V.F. Mathcad 14 dlja studentov, inzenerov i konstruktorov. S-Pb.: BHV- Peterburg.2007. 368 s.
22. Innovacionnij patent № 26454 RK. Sposob pererabotki ferrophosphora / Shevko V.M., Serzanov G.M., Lavrov B.A. Bul. № 12. -2012.-3 s.

**Study of the structural characteristics chemical and phase composition phosphorus sludge**

**Nazarbek Ulzhalgas B.**

PHD-doctoral Univ. CTIS South Kazakhstan State University. M. SKSU, Kazakhstan, Shymkent

**Besterekov Uilesbek Besterekovich**

Professor, Doktor of Sciens, Univ. CTIS South Kazakhstan State University. M. SKSU, Kazakhstan, Shymkent

**Petropavlovsky Igor Aleksandrovich**

Professor, Doctor of Science, Univ. technology of inorganic substances Russian Chemical-Technological University. D. Mendeleev

125047, Russia, Moskow, Miusskaya square, 9

e-mail: [ipetropavlovskiy@gmail.ru](mailto:ipetropavlovskiy@gmail.ru)

**Pochitalkina Irina Alexandrovna**

Associate Professor, Ph.D., Univ. technology of inorganic substances Russian Chemical-Technological University. D. Mendeleev

125047, Russia, Moskow, Miusskaya square, 9

e-mail: [pochilkina@list.ru](mailto:pochilkina@list.ru)

**Keywords:** phosphorus sludge, grain size, elemental, phase composition, microstructure.

**Abstract.** The results of sieve analysis, physico-chemical and microscopic examination of phosphorus sludge. Found that particle size distributions phosphorus sludge does not meet the regulatory requirements for mineral fertilizers. On the chemical composition phosphorus sludge is close to the original raw Karatau phosphate deposits, but differs from it in less phosphate content and the presence of components of the feedstock mass - quartzite and coke. The results of microscopic examination showed that the structure of the phosphor slurry advantageously contains calcium silicates, potassium aluminum silicates and diopside. Based on the work performed can be concluded that phosphorus sludge is a valuable secondary raw phosphate suitable for processing in complex mineral fertilizer.

**References**

1. Chemical technology of inorganic substances. / Ed. T.G. Akhmetov-M.: Chemistry, 1998.

2. Posin M.E. Technology of mineral salts and fertilizers. / / Khimiya, 1986

3. Postnikov N.N. Thermal phosphoric acid. / / Moscow: Khimiya, 1972, 308c.

4. V.A. Ershov, S.D. Pimenov. Electroheat phosphorus. / / St. Petersburg, Chemistry, 1996, 234c.

5. Bat’kaev R.I. Development of technology for commodity products from industrial waste products of phosphorus: summary of doctor of technical sciences, South Kazakhstan State University. M. Auezov, Shymkent, 2010.

6. Instruction of SPECORD 75 IR, production CARLZEISS, ZENA

7. Mineral fertilizers. Test methods: Sat Guest. - Moscow: Publishing PKI standards, 2003.

8. Phosphates in the XXI century. / Ed. Y.A. Kiperman - 208c. Almaty-Taraz-Zhanatas, 2006.

9. V.G. Gorshkov, V.V. Timashev, V.G. Saveliev. Physical-chemical analysis of binders. / Tutorial. / / Moscow: Higher School, 1981, 333s.

**Modeling the process of obtaining tetraalkylammonium hydroxides of high purity by ion exchange**

Konovalov A.N\*., Kotova N.V\*., Grenberg E.E\*., Makarov V.V\*\*.

\*FGUP «IREA», Russia, Moscow

\*\*RXTU im. D.I. Mendeleeva, Russia, Moscow

**Alexander N. Konovalov**, FSUE “IREA”, Chief of Laboratory, e-mail: [solstorm@mail.ru](mailto:solstorm@mail.ru)

**Natalia V. Kotova**, FSUE “IREA”, Researcher, e-mail: fidgety@bk.ru

**Eugene E. Grinberg**, FSUE “IREA”, Deputy director, Professor, e-mail: ireon@mail.ru

**Vladimir V. Makarov**, Russian Chemico-Technological University, Professor, tel. +7 (495) 495-21-17

**Keywords**: tetraalkylammonium bases, ion exchange, modeling

**Abstact.** The process of tetraalkylammonium hydroxides synthesis with ion exchange in periodic column apparatus was studied. Developed a refined model of the ion exchange column of the periodic fixed-bed ion exchanger. The model takes into account the kinetics of internal diffusion in the pores of the resin beads and the effect of longitudinal mixing. The model used to describe the synthesis of high purity tetraalkylammonium bases in column apparatus. Numerical values ​​of internal diffusion halide- and hydroxy- ions coefficients were determined. Experiments on the production of tetraalkylammonium hydroxides model showed good agreement with the results obtained, which confirms the correctness of its choice.

**References**

1. Dolgonosov A.M., Voloshik I.N., Senyavin M.M. Ionniy obmen I ionnaya khromatografiya, RAN, Institut geohimii i analiticheskoi himii im. V.I.Vernadskogo –M.: Nauka,1993.- 312 s.

2. Venetsianov E.V., Dinamika sorbtsii is zidkih sred / E.V.Venetsianov, R.N.Rubinshtein – M.: Nauka, 1983. -237 s.

3. Crank J. The mathematics of diffusion – London: «Oxford university press», 1975 – 415 с.

4. Tevlina A.S. Laboratornii praktikum po himii I tehnologii ionoobmennih materialov: Uchebnoe posobie/ A.S.Tevlina, L.B.Zudakova, Yu.A.Leikin.- M.: RHTU im. D.I.Mendeleeva, 1972.-156 s.

5. Geivandov I.A. Oprebelenie dinamicheskih harakteristik natrii-kationitnogo umyagcheniya mineralizovannih vod po experimentalnim dannim na osnove matematicheskoi modeli/ I.A.Geivandov, N.I.Stoyanov, A.I.Voronin, A.N.Visloguzov, D.V.Kremlev, D.V.Abornev, M.Yu.Kalinlchenko // Neftepromislovoe delo. #11.-M.: OAO “VNIIOENG”, 2005=S.71-74/

6. Stoyanov N.I. Rezultati experimentalnih issledoanii dinamiki parnogo ionnogo obmena pri umyagchenii mineralizovannih vod I metodika rascheta fisiko-himicheskih parametrov prtsessa/ N.I.Stoyanov, I.A.Geivandov, A.I.Voronin, A.N.Visloguzov, D.V.Kremlev, D.V.Abornev, M.Yu.Kalinichenko// Vestnik SevKavGTU, 2006, #27-30.

7. Vorob`yev A.H. Diffuzionnie zadachi v himicheskoi kinetlke/: MGU Himfak.- 2003/- C/19 – 53.

8. Koshkin N.I., Shirkevich M.G. Spravochnik po elementarnoi fizike. M.: Nauka. 1972. – 256 s.

9. Koshel` N.D., Magdich E.A., Akimov A.M. Matematicheskoe modelirovanie protessa regeneratsii ionita v ionoobmennoi kolonke// Voprosi himll I himicheskoi tehnologii.-2008.- #1.- S.152 -155.

10.Sed`moe izdanie:”Kratkii spravochnik fiziko-himicheskih velichin” pod redaktsiei K.P.Mischenko I A.A.Ravdelya. L.: Himiya. 1974.-200 s.

11.Terehov S.V. Modelirovanie teplovih I kineticheskih svoistv real`nih system.Donetsk: “Veber”, 2007.-306 s.

12. Stark J. Diffusiya v tverdih telah. Per. s angl. Moskva “Energiya”. 1980.-239 s.

13. Gupta Renu, Bansal Ajay. Effect of Bed Configuration on Dispersion in a Packed-Bed Reactor/ Ind. And Eng. Chem. Res., 49, №19, 2010. – С. 9525 – 9528.

14. Laboratornii praktikum po protsessam I apparatam himicheskoi tehnologii: ucheb. Posobie. Pod red. prof. G.S.D`yakonova – Kazan`.: Gos tehnol.un-t. Kazan`, 2005/-236 s.

15. Kafarov V.V., Glebov M.B. Matematicheskoe modelirovanie osnovnih protsessov himicheskih proizvodstv. M:, Vishaya shkola, 1991. – 1991. – 367 s.

16. Natareev S.V. Sistemnii analiz i matematicheskoe modelirovanie protsessov himicheskoi tehnologii: ucheb. posobie/S.V.Natareev, pod red. V.N.Blinicheva: Ivan. Gos. him.-tehnol. un-t: - Ivanovo, 2007. – 80 s.

**Investigation of mixing reactants in alkylation of benzene with ethylene using methods of computational fluid dynamics**

**E.Ivashkina\*, E.Khlebnikova, A.Becker, N.Belinskaya, V.Tkachev**

Tomsk Polytechnic University

JSC «Angarskiy zavod polimerov»

\*National Research Tomsk Polytechnic University, 634050, Russia (Tomsk, Lenin Avenue, 30), e-mail: ivashkinaen@tpu.ru, phone +7(3822)705016

**Ivashkina Elena**

Tomsk Polytechnic University, Department of Fuel Engineering and Chemical Cybernetics, Doctor of Technical Sciences, Professor

Address: 634050, Tomsk, Lenin Avenue, 30

Tel: +7 (3822) 705016, e-mail: ivashkinaen@tpu.ru

**Khlebnikova Elena**

Tomsk Polytechnic University, Department of Fuel Engineering and Chemical Cybernetics, the 1st year PhD student

Address: 634050, Tomsk, Lenin Avenue, 30

Tel: +7 (3822) 705016, e-mail: elena.khle@gmail.com

**Belinskaya Nataliya**

Tomsk Polytechnic University, Department of Fuel Engineering and Chemical Cybernetics, the 2nd year PhD student

Address: 634050, Tomsk, Lenin Avenue, 30

Tel: +7 (3822) 705016, e-mail: ns\_belinskaya@sibmail.com

**Alexander Bekker**

Tomsk Polytechnic University, Department of Fuel Engineering and Chemical Cybernetics, the 4th year student

Address: 634050, Tomsk, Lenin Avenue, 30

Tel: +7 (3822) 705016, e-mail: avb6@tpu.ru

**Vladislav Tkachev,**

JSC "Angarsk Polymer Plant", chief of Alkylation Department

Tel: +7 (3955) 574026, e-mail: kobra.1976@mail.ru

**Keywords:** alkylation of benzene, catalyst complex, ethylbenzene, mixing, simulation.

**Abstract.** The purpose of this work is to numerically research benzene alkylation with ethylene and assess a feasibility of the alkylation reactor mixing equipment reconstruction using methods of computational fluid dynamics. To evaluate the effectiveness, a simulation of the mixing chamber was developed using ABAQUS and FlowVision software systems. It allows solving problems with high accuracy in fluid dynamics modeling of liquid and gas flows mixing. Two variants of benzene and catalytic complex input to chamber were considered. Results are presented in color schemes. The obtained results describe the change of reactant concentrations gradient.

**References**

1. Timofeyev V.S. Printsipy tekhnologii osnovnogo organicheskogo i neftekhimicheskogo sinteza: Uchebnoye posobiye dlya vuzov – 2nd edition, pererab. – M.: Vysshaya shkola, 2003.
2. Proizvodstvo i rynok etilbenzola v Rossii // Yevraziyskiy khimicheskiy rynok. – 2011 – №1. – p.48-50.
3. Dolganova I.O., Belinskaya N.S., Ivashkina E.N., Martem'yanova E.V., Tkachev V.V. Povysheniye effektivnosti tekhnologii polucheniya etilbenzola s ispol'zovaniyem metoda matematicheskogo modelirovaniya // Fundamental'nyye issledovaniya. – 2013. – № 8 (3rd part). – p. 595-600
4. Noskov A. S. Vychislitel'naya gidrodinamika v razrabotke kataliticheskikh reaktorov // Sovremennyye tekhnologii i modelirovaniye protsessov pererabotki uglevodorodnogo syr'ya: materialy Vseros. nauch.-prakt. konf., posvyashch. 75-letiyu so dnya rozhdeniya Zasluzhennogo deyat. nauki RF, prof. A. V.Kravtsova, Tomsk, 1–3 okt. 2013. – Tomsk : TPU, 2013. – p. 11–12.
5. Tekhnologicheskiy reglament proizvodstva etilbenzola tsekha 126/127 JSC «Angarskiy Zavod Polimerov».
6. Modelirovaniye trekhmernykh statsionarnykh i nestatsionarnykh techeniy zhidkosti i gaza [electronic resource]: <http://www.flowvision.ru/>
7. Chizhiumov S. D. Osnovy gidrodinamiki. – Komsomol'sk-na-Amure : KnASTU, 2007.
8. Korkodinov YA. A. Obzor semeystva k – e modeley dlya modelirovaniya turbulentnosti // Perm National Research Polytechnic University: <http://vestnik.pstu.ru>