Development of a method of dehydration triple system LiOH - H2O2 - H2O for lithium peroxide

Ferapontov Uri Anatolevich, Senior researcher Tambov State Technical University

Russia, Tambov,st. Sovetskya, 106; e-mail: mail@roshimzaschita.ru

Nefedov Roman Andreevich, Senior researcher Tambov State Technical University

Russia, Tambov, st. Sovetskya, 106;e-mail: kliorik@mail.ru

Keywords: dehydrations of threefold system КOH – H2O2 – H2O, alkali metals peroxidates, regenerative products, hardware - technological design, heating in the infrared range, microwave field.

The theoretical analysis practically all ways of receiving peroxide compound of lithium (Li2O2) known for today is carried out. It is shown that for development of an easy way of receiving Li2O2 capable to be realized in the commercial scale, it is expedient to carry out a dehydration of the threefold LiOH system – H2O2 – H2O. The optimum route of process of receiving peroxide compound of lithium – through formation of the intermediate adduct of structure of Li2O2∙H2O is theoretically reasonable. The method of solubility established temperature and concentration areas of a crystallization of the Li2O2∙H2O connection from the LiOH system – H2O2 – H2O. The way of receiving peroxide compound of lithium by a dehydration by means of the microwave oven of radiation of the threefold LiOH system – H2O2 – H2O is offered and the optimum technological parameters of process allowing to receive termination products with the content of peroxide compound of lithium to 97% are determined. Lithium peroxide compound synthesis realization from hydrogen peroxide and oxyhydroxide of lithium under the conditions described in work allowed to refuse a stage of separation of a solid phase from a mother solution that not only reduces losses of ions of lithium to technologically necessary minimum, but also to simplify and intensify synthesis process.

References

1. Presti J., Wallman H., Petroctlli A. Superoxide life support system for submersibles. Undersea Technol., 1967, Vol.8,pp.20 - 25.

2. Voronin G. I., Polivoda A. I. Life support of crews of spaceships. М.: Mashinostroenie, 1967,p.36. (in Russ.).

3. Petroctlli A., Capolesto A. Some notes on the use of superoxides in regenerative air system.Aerospase Med., 1964, Vol.31, pp. 440 - 447.

4.Didenko N. S.Regenerative respirators for mine-rescue works. М.: Nedra, 1984, p.68. (in Russ.).

5.Bujanov V. V., Suprun I. P. Individual protection equipment for works in microbiological and virologic laboratories. Chernogolovka, IPHF, 2001,p.324. (in Russ.).

6. Dobrynina T. A. Lithium peroxide. M.:Nauka, 1964, p.52. (in Russ.).

7. VolnovI. I. Peroxidates of alkali metals. M.: Nauka. 1980. p.160. (in Russ.).

8. F. Albert Cotton. Progress in Inorganic Chemistry.Interscience Publishers. Vol. 4, New-York – London, 1962, 247 p.

9. Rilley J. F. Thermal Decomposition of Potassium Oxides in the Temperature range 300 - 4800C. Dissertation. Univ. Rhode Island, 1968.

10. Firsova T. P., Molodkina A. N., Morozova T. G. i dr. About melting point of of a potassiumsuperoxide.Izvestija AN SSSR, OHN, [News SA USSR]1965, № 9, pp. 1678 - 1680. (in Russ.).

11. Tsentsiper A. B., Rogozhnikova T. I. To a question of potassium superoxide melting. Izvestija AN SSSR[News SA USSR] Serija him., 1967, № 1, pp. 195 - 197. (in Russ.).

12. FerapontovYu. A., GladyshevN. F., UljanovaM. A.. Regenerative products of new generation: technology and instrument registration. M.: Mashinostroenie - 1, 2007. p.156. (in Russ.).

13. Strater H. H., Heights M.Method of making lithium peroxide in methanol. US № 2962358, NKI 23-184, 1960.

14. Bach R. O., Boardman W. W.Process for producing anhydrous lithium peroxide by the use of a substantially water – immiscible organic liquid. US № 3147075. NKI 23-184, 1964.

15. Klebba E. L. Preparation of alkali metal peroxides. US № 3212850. NKI 23-184, 1965.

16. Bach R. O.Preparation lithium perox-ides. US № 3134646. NKI 23-184, 1964.

17. Winternitz P. Preparation of anhydrous lithium peroxide. US № 2488485. NKI 23-184, 1949.

18. Smith W. N. Method for preparing lithium peroxide.US № 3446588. NKI 23-184, 1969.

19. Ferapontov Yu.A., Simanenkov S. I., Gladyshev N.F., Putin B.V. Way of receiving peroxide compound of lithium. RU №2193522, 2002. (in Russ.).

20. Ferapontov Yu. A., Simanenkov S.I., Gladyshev N. F. Development of waste-free technology of receiving peroxide compound of lithium. Himicheskajatehnologija [Chemical technology], 2004, № 4, pp. 2. – 7. (in Russ.).

21. Makarov S. Z., Dobrynina T. A. Studying of systems with concentrated hydrogen dioxide. Message 9. The threefold LiOH system - H2O2 - H2O. Izvestija AN SSSR[News SA USSR],OHN, 1955, №3, pp. 411 - 414.(in Russ.).

22. Makarov S. Z., Dobrynina T. A. Studying of systems with concentrated hydrogen dioxide. Message 11. A thermal characteristic of solid phases of the LiOH system - H2O2 - H2O.Izvestija AN SSSR [News SA USSR], OHN, 1956, №3, pp. 294 - 298. (in Russ.).

23. Dobrynina T. A. Solubility isotherm at 30,5°C of the threefold system LiOH - H2O2 - H2O and studying of hydrated peroxide of lithium. Izvestija AN SSSR [News SA USSR], OHN, 1960, №6, pp. 961 - 964. (in Russ.).

24. Ferapontov Yu. A., Ul'janova M. A., Sazhneva T. V., Kozlova N. P. Studying of a kinetics of disintegration of a liquid phase of the threefold system LiOH – H2O2 – H2O in the presence of a solid phase of structure of Li2O2∙H2O. Zhurnalprikladnojhimii [Journal of Applied Chemistry],2008, T. 81. V. 1, pp. 28 - 31. (in Russ.).

25. Ferapontov Yu. A., Ul'janova M. A., Sazhneva T. V. Parameters of Li2O2 H2O Crystallization from the LiOH – H2O2 – H2O Ternary System. Russian Journal of Inorganic chemistry, 2008, Vol. 53, № 10,pp. 1635 – 1640.

26. Ferapontov Yu. A., Ul'janova M. A., Sazhneva T. V.Conditions of a crystallization of Li2O2∙H2O in the threefold system LiOH – H2O2 – H2O. Zhurnalprikladnojhimii [Journal of Applied Chemistry],2008, T. 53, V. 10, pp. 1749 - 1754. (in Russ.).

28. Shmakov A. N., Bodazhkov V. A. Projection and operation of high-pitched installations. L.: Mashinostroenie, 1978, p.280. (in Russ.).

29. DorohovI. N., Mel'nikovV. V. Systems analysis of processes of engineering chemistry.M.:Nauka, 2005, p.584.

30. FerapontovYu.A., M. A. Ul'janova, T. V. Sazhneva.Way of receiving peroxide compound of lithium. RU № 2322387, 2008. (in Russ.).

31. Seyb E., Kleinberg J. Determination of superoxid oxygen. J. Am. Chem. Soc. 1951,V. 73, pp. 2308 - 2314.

32. Alekseevskij G. V., Gol'ts R. K., Musakin A. A. The quantitative analysis. M.: Goshimizdat, 1955,p.558. (in Russ.).

Technological design of process of the dehydration of the threefold system KOH– H2O2 – H2O for receiving the regenerative product on the matrix

Ferapontov Uri Anatolevich, Senior researcher Tambov State Technical University

Russia, Tambov,st. Sovetskya, 106; e-mail: mail@roshimzaschita.ru

Nefedov Roman Andreevich, Senior researcher Tambov State Technical University

Russia, Tambov, st. Sovetskya, 106;e-mail: kliorik@mail.ru

Dorohov RomanViktorovich

Public JSC "Corporation «Roschimzaschita»,

Head of laboratory of department ofchemistry and innovative chemical     technologies

Russia, Tambov, Morschanskoye highway, 19,

Phone: (4752) 56-06-80,

e-mail: mail@roshimzaschita.ru.

Keywords: dehydrations of threefold system КOH – H2O2 – H2O, alkali metals peroxidates, regenerative products, hardware - technological design, heating in the infrared range, microwave field.

Various routes of chemical reactions in the preparation of potassium superoxide ternary system  KOH - H2O2 - H2O. Theoretically justified, that in order to obtain the final product with maximum content of potassium superoxide  must rapid removal of water vapor from the reaction zone.  On the basis of the analysis of various methods of a dehydration of the threefold system KOH – H2O2 – H2O for receiving a regenerative product on the basis of a potassium superoxide is carried out the choice ofa hardware – technological process. The assessment of effectiveness of the considered methods in the following parameters is carried out: efficiency, profitability and the maintenance  of a potassium superoxidе in a synthesis product. The received results allow to draw a conclusion that ways of receiving a regenerative product on a porous matrix in current of the drained and heated air and receiving a regenerative product on a porous matrix heating by resistance will be the most perspective for realization in the commercial scale.

References

1.Presti J., Wallman H., Petroctlli A. Superoxide life support system for submersibles. Undersea Technol.,1967, Vol.8,p.20.

2. Ivanov D.I., Hromushkin A.I. Life support systems for high-altitude and aerospace flights. M.: Mashinostroenie, 1968, p.61. (in Russ.).

3. Petroctlli A., Capolesto A. Some notes on the use of superoxides in regenerative air system. Aerospace Med., 1964, Vol.31,p. 440.

4. FerapontovYu.A., Gladyishev N.F., Ulyanova M.A. idr. Regenerative products of new generation: technology and instrument registration.M.: Mashinostroenie- 1, 2007, p. 156. (in Russ.).

5. Volnov I. I. Peroxidates of alkali metals. M.: Nauka, 1980,p.161 (in Russ).

6. Kazarnovskiy I.A. Neyding A.B. Research of the mechanism of decomposition of hydrogen dioxide in some solid pergidrata. Dokladyi AN SSSR [Reports AN USSR], 1952, T. 86.№ 4, p.717. (in Russ.).

7. Kazarnovskiy I.A. About the hydrogen dioxide autodecomposition mechanism.Dokladyi AN SSSR [Reports AN USSR], 1975, T. 221,№ 2,p.353. (in Russ.).

8. FerapontovYu.A., Zhdanov D.V., Ulyanova M.A.Research of kinetics of process of receiving potassium superoxide of an alkaline solution of hydrogen peroxide.Zhurnalprikladnojhimii [Journal of Applied Chemistry], 2005, T. 78, V.2.pp. 191 - 194. (in Russ.).

9. FerapontovYu.A., Ulyanova M.A., Putin S.B. The choice of optimum conditions of receiving a potassium superoxide from hydrogen peroxide and potassium hydroxide in the reactor of spraying type.Himicheskayatehnologiya [Chemistry technology], 2008, T. 9,V.8,pp. 357 - 364. (in Russ.).

10. Gladyishev N.F., Glebova O.N., Andreev V.P., Putin B.V. Regenerative product and way of its receiving.RU 2225241, 2004. (in Russ.).

11. Gladyishev N.F., Simanenkov E.I., Dorohov R.V. i. dr. Development of the self-rescuer of the emergency protection of the civilian population at the emergency situations.Himicheskayaibiologicheskayabezopasnost [Chemical and Biological Safety], 2012, T.1-2, pp. 90 – 95. (in Russ.).

12. Gladyishev N.F., Dorohov R.V., PlotnikovM.Yu. i. dr. Blok of chemical regeneration of air.Himicheskayaibiologicheskayabezopasnost [Chemical and Biological Safety], 2012, T.1-2,pp. 96 – 99. (in Russ.).

13. Dorohov R.V., Gladyishev N.F., Dvoretskiyi.dr.Kinetics of interaction of carbon dioxide with potassium superoxide.Himicheskayafizika [Chemical physics], 2007, T.26, V.10,pp. 81-84.(in Russ.).

14. Dorohov R.V., Gladyishev N.F., Dvoretskiy S.I. i. dr. Searching of paths of an intensification of process of receiving a regenerative product on a matrix in vacuo. VestnikTGTU [MessengerofTGTU], 2006, T.12, №.4A,pp. 1057-1064. (in Russ.).

Prospects of production of activated carbon from rice husk in Vietnam

Korobochkin Valeriy Vasiljevich, DSc, professor of the Department of General Chemistry and Chemical Engineering, Institute of High Technology Physics, National Research Tomsk Polytechnic University (634050 Russia, Tomsk, Lenin avenue, 30), E-mail: vkorobochkin@tpu.ru

Nguyen Manh Hieu, postgraduate student of the Department of General Chemistry and Chemical Engineering, Institute of High Technology Physics, National Research Tomsk Polytechnic University (634050 Russia, Tomsk, Lenin avenue, 30), E-mail: kqhak@yandex.ru

Usoltseva Natalya Vasiljevna, senior lecturer of the Department of General Chemistry and Chemical Engineering, Institute of High Technology Physics, National Research Tomsk Polytechnic University (634050 Russia, Tomsk, Lenin avenue, 30), E-mail: usoltseva.nv@mail.ru

Nguyen Van Tu, DSc, professor of the School of Materials Science and Engineering, Hanoi University of Science and Technology, 1 Dai Co Viet, Hanoi, Vietnam. E-mail: tu.nguyenvan@hust.edu.vn

Keywords: rice husk, composition, heat treatment, hydrocarbon, activation, the specific surface area.

Patterns of change in the composition of rice husk during heat treatment in a stream of air and Argon by using thermal analysis combined with mass spectrometry and IR spectroscopy were investigated. During pyrolysis in flowing argon at 550 °C, an increasing of carbon content from 40.80 to 44.10 %, reduction in oxygen content from 44.82 to 26.17 % wt. and a significant increase in silicon content from 7.00 to 25.00 % wt. were observed in comparing with the source material. Activation of materials which were obtained after carbonization and separation of silica was carried out using water vapor and carbon dioxide at temperatures from 700 to 850 °C. The result showed that the highest value of specific surface area was achieved at 1345 m2/g when the activation was performed at temperature 850 °C and when the flow rat References

1. General statistics office of Viet Nam URL: https://gso.gov.vn/default.aspx?tabid=717

2. Kalderis D., Bethanis S., Paraskeva P. Production of activated carbon from bagasse and rice husk by a single-stage chemical activation method at low retention times. Bioresource Technology, 2008, vol. 99, is.15, p. 6809–6816.

3. Foo K.Y., Hameed B.H. Utilization of rice husks as a feedstock for preparation of activated carbon by microwave induced KOH and K2CO3 activation. Bioresource Technology, 2011, vol. 102, is. 20, p. 9814–9817.

4. Tzong-Horng Liou. Preparation and characterization of nano-structured silica from rice husk. Materials Science and Engineering, 2004, vol. 364, p. 313–323.

5. Witoon T., Chareonpanich M., Limtrakul J. Synthesis of bimodal porous silica from rice husk ash via sol–gel process using chitosan as template. Materials Letters, 2008, vol. 62, is. 10–11, p. 1476–1479.

6. Yan Liu, Yupeng Guo, Yanchao Zhu. A sustainable route for the preparation of activated carbon and silica from rice husk ash. Journal of Hazardous Materials, 2011, vol. 186, is. 2–3 p. 1314–1319.

7. Dongmin An, Yupeng Guo, Bo Zou. A study on the consecutive preparation of silica powders and active carbon from rice husk ash. Biomass and Bioenergy, 2011, vol. 35, is. 3, p. 1227–1234.

8. GOST 6217-74. Ugol aktivnyiy drevesnyiy droblenyiy. Tehnicheskie usloviya [Wood crushed activated carbon. Specifications]. Moscow: Standards Publishing House, 2003, 7 p (in Russ.).

9. Zhbankov R.G. Infrared spectra and structure of carbohydrates. // Minsk, Nauka i tekhnika [Science and Technology], 1972, 456 p (in Russ.).

10. Efremova S.V. Physical and chemical bases and technology of thermal processing of rice husk. // Almaty, 2011, 149 p (in Russ.).

11.	Marsh H., Rodriguez-Reinoso F. Activated Carbon. // Elsevier Science & Technology Books, 2006, 530 с.

12. Dang Nhan Thong, Nguyen Manh Hieu, Korobochkin V.V. Analysis of the combustion process in the production of activated carbon. Nauchno-tehnicheskiy i proizvodstvennyiy zhurnal «Nanoinzheneriya» [The Monthly Scientific and Production Journal «Nano Ingineering»], 2014, no. 11, pp. 36-38 (in Russ.).

13.	Hieu N.M., Korobochkin V.V., Tu N.V. A Study of Silica Separation in the Production of Activated Carbon from Rice Husk in Viet Nam. Procedia Chemistry, 2015, vol. 15, p. 308-312.

14. Ismail A.F., Khulbe K., Matsuura T. Gas Separation Membranes: Polymeric and Inorganic, Springer International Publishing, 2015, 331 p.

Calculation of the reverse osmosis installation for desalination of the Black and Caspian seas

Zhilin Yuriy  Nicolayevich Moscow state technical university named after N.E. Bauman, Associate Professor, Department of chemistry.

Address: 141005, Mytishchi-5, Moscow region, Institutskaya, 1.

Tel. 8(498)687-36-00

e-mail: Iouri-Jiline@yandex.ru

Keywords: reverse osmosis, baromembrane process, spiral wound membrane element, desalination.

The efficiency of reverse osmosis desalination of the black sea and the Caspian sea waters were. The calculations were performed with respect to the spiral wound element BW30-400 Filmtec company.  The water of the seas was simulated by NaCl solutions, 18 and 12 kg/m3 respectively. The maximum allowable concentration of salt in desalinated water (permeate) was limited to 0.5 kg/m3. We performed the calculations using the mathematical model of separation, which took into account the influence of the concentration polarization along the length of the discharge channel. The calculations with a minimizing the energy consumption were carried out. Calculation results show that desalination of the black sea water is advantageously carried out at following values of parameters: absolute operating pressure at the inlet of the element is 29 bar and the flow rate at the inlet of the discharge channel is 0.015 m/s. In this case, the volume fraction of desalinated water is almost half that of the source and equal 0,441, and the salt concentration does not exceed 0,471 kg/m3. At the same flow rate, 0,015 m/s, Caspian water desalination indicators are above:  25 bar, 0,56 and 0,224 kg/m3 respectively. This is due to its lower salinity compared to the Black sea water.

References

1. Dytnerskiy Yu.I. Baromembrannye protsessy. Teoria i raschet. [Baromembrane processes. Theory and calculation]. – M.: Khimiya  [Chemistry]. 1986. 272 p. ( in Russ ).

2. Svitsov A.A. Vvedenie v membrannye tekhnologii [Introduction to metmdrane technology]. M.,: DeLi print. 2007, 280 p. ( in Russ ).

3. Lisa Henthome, Buddy Boysen. State-of-the-art of reverse osmosis desalination pretreatment. Desalination,  v 356, 15 January 2015, p.p. 129 – 139.

4. Reverse-osmosis membranes. www.inaqua.de

5. Zhilin Yu.N. Matematicheskaya model i raschet rulonnogo obratnoosmoticheskogo elementa [Matemaical model and calculation of spiral wound reverse osmosis element]. / Saarbrucken, Lambert Academic Publishing, 2016, 66 p, ISBN 978-3-659-84802-5. ( in Russ ).

6. Zhilin Yu.N. Vliyanie skorosti potoka na razdelenie rastvora NaCl v obratnoosmoticheskom rulonnom elemente. [Effect of flow rate on separation of NaCl solution in a spiral wound reverse osmosis element]. Vestnik MGUL – Lesnoy vestnik [Moscow state forest university bulletin – Lesnoy vestnik] 2015, т.19,  № 6, p.p. 126 –  131. ( in Russ ).

7. Popov N.I., Fedorov K.N., Orlov V.M. Morskaya voda. Spravochnoe rukovodstvo (pod. red. Monina A.S.) [Sea water. Gide book (ed. Monin A.S.)]. – M., Nauka [Science], 1979, 327 p. ( in Russ ).

8. Skopintsev B.A. Formirovanie sovremennogo himicheskogo sostava vod Chernogo morya [Contemporary chemical composition formation of Black sea water]. – L., Gidrometeoizdat, 1975, 336 p.   ( in Russ ).

9. Zhilin Yu.N. Baromemdrannoe razdelenie rastvora v ploskom shtshelevom kanale. Matematicheskoe opisanie i primer raschyota obratnoosmoti-cheskogo rulonnogo elementa [Baromembrane separation of solution in a flat slop channel. Mathematical description and calculation example of spiral wound reverse osmosis element]. Khimicheskaya promyshlennost segodnya [Chemical Industry Today],  № 4, 2015, p.p. 33 – 43.   ( in Russ ).

10. Shlyamin B.A. Kaspiyskoe more [Caspian Sea].– M., Geografgiz, 1954, 128 p.

11. Dobrovolskiy A.D., Zalogin B.S. Morya SSSR [USSR Seas]. – Izdatelstvo Moskovskogo universiteta [Moscow University edition] 1982, 192p. ( in Russ ).

Mass transfer efficiency at liquid-liquid extraction in the regime of turbulent co-current flow of a film over the packing

Farakhov Timur Mansurovich

Engineering and innovation center «Ingehim», engineer,

address: 420049, Kazan, Shalyapina st. 14/83; e-mail: info@ingehim.ru

Laptev Anatoliy Grigorievich

“Kazan State Power Engineering University”

Аddress: 420066, Kazan, st. Krasnoselskaya d.51

Tel.rab: (843) 519-42-54; e-mail: tvt_kgeu@mail.ru

Keywords: turbulent co-current flow, liquid-liquid extraction, cell model.

For increasing efficiency of liquid-liquid extraction, the method of interaction of phases in case of a turbulent concurrent flow in the channel filled with random packing is considered. Such design can be a substitute for an apparatus with a mechanical mixer or, alternatively, it can be used for increasing separation ability of an existing gravitational extractor. In case of an assumption that the disperse phase wets a surface of packing elements sufficiently well, the cell model for the fluid flow structure containing volumetric sources of mass is provided. The expressions for determining the mathematical model parameters such as mass transfer coefficients and the number of cells of complete mixing are given. Required experimental information regarding the channel filled with packing is hydraulic resistance. Results of calculations of mass transfer efficiency depending on Reynolds number are shown. A conclusion is drawn regarding the most rational extraction mode providing sufficient efficiency and a small pressure drop.

References

1. Laptev A.G., Dudarovskaya O.G., Farakhov T.M. Model of mass transfer in liquid-liquid extraction in a turbulent forward flow. Ingenerno-Fizicheskiy Jurnal [Journal of Engineering Physics and Thermophysics], 2015, v. 88, no. 1. pp. 207–213

2. A.G., Dudarovskaya O.G., Farakhov T.M. …. Liquid-liquid extractor. RU 2015129216/05, 2016

3. Aerov M.E., Todes O.M., Narinskii D.A. Apparatuses with the stationary granular bed. – L.: Khimia, 1979. 176 p. (in russ)

4. Komissarov Yu.A., Gordeev L.S., Vent D.P. Processes and apparatuses of chemical technology, textbook for universities. M.: Khimiya, 2011. 1230 p. (in russ.)

5. Laptev A.G., Farakhov T.M., Dudarovskaya O.G. Models of turbulent viscosity and mixing in channels and packed flow-through mixers. Russian Journal of applied chemistry. 2013, v. 86. no. 7. pp. 1046–1055

6. Laptev A.G. Transport models and liquid extraction efficiency.Kazan: Kazan State Power Engineering University press, 2005. 229 p. (in russ.)

7. Laptev A.G., Lapteva E.A., Farakhov T.M. Models of transport phenomena in random packed and granular beds Theoretical Foundations of Chemical Engineering, 2015, v. 49. no. 4. pp. 388–395

8. Kadenskaya N.I., Zheleznyak A.S., Brounshtein B.I. Mass transfer in a spray extraction column, in: Processes of Chemical Technology. – M.: Nauka, 1965. pp. 215–218. (in russ.)

Rectification purification of tetraethoxysilane

Belyaev Evgeny Alexandrovich

Scientist	 «ECOS-1» Ltd.

tel. (499) 394-19-21

E-mail: belyaev.ea@gmail.com

Beerngarten Mihail Georgievich

PhD, Professor, Department chair MAMI

E-mail: belyaev.ea@gmail.com

Grinberg Evgeny Efimovich

Doctor of Chemistry, Director advisor «ECOS-1» Ltd.

Keywords: purification, tetraetoxysilane, TEOS, rectification.

Established principle possibility of tetraetoxysilane (TEOS) cleaning by rectification. Proved possibility of a continuous process of rectification purification.It was found that the purification of TEOS from the impurities of non-transition elements is effective at low reflux ratio in the columns with a small number of theoretical plates of cleaning. Proved the possibility of a continuous process of distillation purification. As a result of work it was established that the formation of impurities alkoxides of transition elements or complex alkoxides vire possible with low partition coefficient in the system 'liquid-vapor'. It is established that during the distillation TEOS process is necessary to prevent its long delay in start of the apparatus due to the polymerization process, even in the absence of water in the system. The best time of the process is less than five hours.

References

1.  Elyseeva L.E. A study of the reactions of monosilane by disproportionation triethoxysilane. – Doctor thesis - М., 1967, 220p. ( in Russ).

2. Ryabenko Е.А., Kyznetsov А.I., Shalumov B.Z. Creating a process of deep cleaning process tetraethoxysilane. – Thesis abstract, Gorky, 1976, 133p. ( in Russ).

3. Grynevich К.P., Suhov А.F. The continuous method for obtaining the ethyl ester of orthosilicic acid. – Plastmassy [Plastic mass], 1959, №2, p. 39-41 ( in Russ).

4. Feld R., Cowe P. The organic chemistry of titanium. - London: Butterworth, 1965, 15 p.

5. Andrianov К.А., Vasyliva Т.V., Korotkevich С.H. Organocyclosiloxanes polymerization reaction with titanium tetrachloride. – Jurnal obshei himii [General chemistry journal], 1962, b.32, p.2311-2314 ( in Russ).

6. Shorygin P.P. General chemistry. - М.: Goshimizdat, 1940. - p. 2190 ( in Russ).

7. Chichibabain А.Е. Main stydu of organic chemistry М.: Goshimizdat, 1960, p. 339-343 ( in Russ).

8. Casey A.T., Clark R.J. Preparations, structures, electronic spectra and magnetism of Vanadium (III) alcoholates. - Inorg. Chem., 1969, v.8, N6, 1218p.

9. Gigauri G.D., Synthesis and some reactions of arsenous acid esters: PhD thesis - Tbilisi, 1971, 20p. ( in Russ).

10. К.А. Andrianov. The process for producing synthetic resins. RU  71115.  1948, №5 ( in Russ).

11. Andrianov К.А., Ganina Т.N., Hrystaleva Е.N. Polyorganostanumsyloxanes and polyorganotitanosyloxanes - Izv. Academy of sciences of USSR, 1956, №7, p. 798-804 ( in Russ).

12. Kreshkov А.P., Mihailenko U.Y., Yakimovich G.F. Determination of the structure of silicone compounds by infrared spectroscopy. - MICTR, 1952, vyp.17, p. 24-33 ( in Russ).

13. Volnov U.N. The study of the interaction of tetraethoxysilane from chlorine, bromine and iodine with stannum. – J. phus.chem., 1955, b.29, e.5, p.1646-1650 ( in Russ).

14. Kreshkov А.P., Chivikova А.N., Nesonova G.D. Double exchange reactions of silicone compounds with inorganic. - MICTR, 1952, b. 17, p. 15-23 ( in Russ).

15. Efremov А.А., Levina Е.F., Zelvenski Y.D. The equal distribution between liquid and vapor trace of phosphorus and tin triethoxysilane. – J. pricl. chem., 1970, b.11, p. 2432-2436 ( in Russ).

16. Ryabenko Е.А., Lastovsky R.P., Blum G.Z. Preparation of high purity kremneetil ether. Reagents and high-clean substances. - М.: NIITEHIM, 1974, p. 62-78 ( in Russ).

17. Е.А. Belyaev, Study treatment with aqueous ammonia solution of tetraethoxysilane // Adstract thesis ХIV Int. conference «Technical sciences  - from theory to practice », 2012, Novosibirsk, p. 91-96. ( in Russ).

18. I.Е.Strelnikova, Е.Е.Grinberg, U.I.Levin, А.Е.Amelina, V.I.Rahlin Sitez of mixed cellosolvate Mg-Si //Inorganic materials, b. 52 № 12, 2016, p.1327-1330.

19. V.М.Retivov, PhD thesis, IREA, 2013, 193 p.. ( in Russ).

20. N.Y.Turova, Metal ocsoalcocsides, Uspehi himii [Successes of chemictry], 73 (11) 2004, p.1132 -  1154 ( in Russ).

21. Y.D.Zelvensky, А.А.Titov, V.А.Shalygin, Dilute solutions rectification, Chemstry,   p. 197. ( in Russ).

Selection of “polymer-solvent-coagulant” system for safe spinning of hollow fiber gas separation membranes

Ivanov Mikhail Vladimirovich

Dmitry Mendeleev University of Chemical Technology of Russia,

Ph. D. student at Isotopes and hydrogen energetic department

Address: 125047, Miusskaya sq. 9, 125047 Moscow;

e-mail: mihail-ivan0v@yandex.ru

Storozhuk Ivan Pavlovich

A.N.Nesmeyanov Institute of Organoelement Compounds of Russian Academy of Sciences (INEOS RAS), senior research associate at laboratory of heterochain polymers

Address: 119991, GSP-1, Moscow, V-334, Vavilova St. 28, INEOS

Tel.: 8 (499) 135-92-02; e-mail: storozhuk-ip@inbox.ru

Dibrov George Albertovich

Dmitry Mendeleev University of Chemical Technology of Russia,

Ph.D, assistant at Membrane technology department

Adress: 125047, Miusskaya sq. 9, 125047 Moscow;

e-mail: george.dibrov@gmail.com

Varezhkin Aleksandr Vladimirovich

Dmitry Mendeleev University of Chemical Technology of Russia,

Ph. D., associate professor at Isotopes and hydrogen energetic department

Adress: 125047, Miusskaya sq. 9, 125047 Moscow;

e-mail: ale-varezhkin@yandex.com

Pavlukovich Nadezhda Gennadievna

A.N.Nesmeyanov Institute of Organoelement Compounds of Russian Academy of Sciences (INEOS RAS), junior research associate of laboratory of heterochain polymers

Address: 119991, GSP-1, Moscow, V-334, Vavilova St. 28, INEOS

Tel.: 8 (499) 135-92-02;

e-mail: pavlukovich@yandex.ru

Kagramanov George Gaikovich

Dmitry Mendeleev University of Chemical Technology of Russia,

Doc., prof., dept. Chairman at Membrane technology department

Address: 125047, Miusskaya sq. 9, 125047 Moscow, Russia

Tel. +7 (499) 978-82-60;

e-mail: kadri@muctr.ru

Keywords: hollow fiber membrane, gas separation, polymer, polymer synthesis, polymer film.

In this paper is carried out the analysis and choice of polymeric membrane materials with optimal gas transport characteristics for air separation, as well as with possibility to be produced into asymmetric hollow fiber membranes from ecologically safe system “solvent-coagulant”. The necessity of synthesis of new polymers which satisfies a complex of exploitation and technological characteristics is vindicated.  Gas separation characteristics of dense film membranes from novel polymers, synthesized at MUCTR of D.I. Mendeleev are studied. One of the synthesized polymers has perspective gas separation properties: ideal separation factor α0(O2/N2)=6,3 and permeability Λ=2,4 Barrer or 8,0·10-16 mol·m/m2·s·Pa.

References

1. Dytnerskiy Yu.I., Brykov. V.P., Kagramanov G.G. Membrane gas separation // М.: Khimia, 1991 (in Russ.).

2. Vinogradov N.E., Talakin O.G., Kagramanov G.G. Membrane separation of hydrogen from off-gas // Khim. prom. Segodnya, 2013, № 5, p. 29 (in Russ.).

3. Papkov S.P. Theoretical foundations of chemical fibers production // М.: Khimia, 1990 (in Russ.).

4. Kesting R.E. Synthetic polymeric membranes// М: Khimia, 1991 (in Russ.).

5. Clausi1 D.T., Koros W.J. Formation of defect-free polyimide hollow fiber membranes for gas separations// J. Mem. Sci, 167, 2000, P. 79.

6. Ekiner O.M., Hayes R.A., Manos P. Reactive post treatment for gas separation membranes// US Patent 5.091.216., E.I. du Pont de Nemours, 1992.

7. Ivanov M.V., Dibrov G.A., Loyko A.V., Varezhkin A.V., Kagramanov G.G.  Techniques to manage geometry characteristics of hollow fiber membranes//  Teor. Osnovy. Khim. Tekhnologii, 2016, V 50,  № 3, p. 325 (in Russ.).

8. Parker Hannifin Manufacturing Netherlands (Filtration and Separation). Analysis of alternatives// 2014, P. 91.

9. Shu-Guang Li. Preparation of hollow fiber membranes for gas separation.

10. Jaap van`t Hof. Wet spinning of asymmetric hollow fiber membranes for gas separation// Enschede, The Netherlands, 1988.

11. Alei P.E., Schletz J.C., Jensvold J.A. Loom processing of hollow fiber membranes// U.S. Patent 5.598.874, MG Generon, Inc., 1997.

12. Sanders D.F., Smith Z.P., Guo R. Energy-efficient polymeric gas separation membranes for a sustainable future: A review// Polymer, 54, 2013, P. 4729.

13. Li Y., Wang X., Ding M., Effects of Molecular Structure on the Permeability and Permselectivity of Aromatic Polyimides// Journal of Applied Polymer Science, 1996, Vol. 61, P. 741.

14. Stern S. A., Walawender, W. P.  Analysis of Membrane Separation Parameters, Separation Science// 1969, V. 4, pp. 129-159.

15. Frolov D.M., Dibrov G.A., Kagramanov G.G., Modelling of membrane air separation in hollow fiber// Uspekhi v khimii I khimicheskoy tehnologii, 2015, V. 29, № 2 (161), P. 107-109 (in Russ.).

About the explosion of some organic compounds with explosive groups

Vasin Alexey Yakovlevich

D.I. Mendeleev University of Chemical Technology of Russia, Professor of Technosphere Safety Department, Doctor of Technical Sciences

Address: 125047, Moscow, Miusskaya Sq., 9

Phone: (495) 948-56-53;

e-mail: vasin-aj@mail.ru

Gadzhiev Garun Gamzatovich

D.I. Mendeleev University of Chemical Technology of Russia, leading Engineer of the Department of Technosphere Safety

Address: 125047, Moscow, Miusskaya Sq., 9

Phone: (495) 948-56-53;

e-mail: garun_jan@mail.ru

Raikova Vlada Myroslavovna

D.I. Mendeleev University of Chemical Technology of Russia, Docent of Technosphere Safety, Candidate of Technical Sciences

Address: 125047, Москва, Miusskaya Sq., 9

Phone: 8 (495) 496-69-73;

e-mail: cherford@yandex.ru

Anosova Evgenya Borisovna

Civil Defence Academy (CDA) EMERCOM of Russia, Docent of Fire Safety Department, Candidate of Technical Sciences

Address: 141435, Moscow region, Khimky, Novogorsk district;

e-mail: evgenia.anosowa@yandex.ru

Shushpanov Alexander

D.I. Mendeleev University of Chemical Technology of Russia, Postgraduate student of the Department of Technosphere Safety

Address: 125047, Москва, Miusskaya Sq., 9;

e-mail: vremena@me.com

Keywords: kinetic parameters of thermal decomposition, the heat of explosion, flash point, the rate of combustion in the Crawford bomb.

The article discusses the explosive properties of mononitroderivates of luminol (5-nitro-2,3-dihydro phthalazine-1,4-dione and its sodium salt) and 1,4-dinitrosobenzene. The article provides fire and explosion hazard characteristics and values of the heats of explosion which were calculated by the programs REAL and SD. Using the method of Kissinger kinetic parameters of the first stage of thermal decomposition of the two compounds were determined. Using the kinetic parameters and heats of explosion according to formula, which is a consequence of solving the problem of thermal explosion in convective heat exchange with the environment, flash point of the compounds were calculated. The velocities of combustion of substances in the Crawford bomb were defined. General conclusion about the explosive properties of the compounds was done.

References

1. Taubkin I.S. Classification of substances by their ability to explosive transformation, VINITI. Problemy bezopasnosti pri chrezvychainykh situatsiyakh [Problems of safety in emergency situations], 1997, no.11, pp. 29-36 (in Russ.).

2. Gadzhiev G.G., Golubeva V.A., Vasin A.Ya. Fire and explosion hazard of some phthalazinedione compounds, Materialy mezhdunarodnoi n/p konferentsii i shkoly molodykh uchennykh «Obrazovanie i nauka dlya ustoichivogo razvitiya» [Materials of international scientific-practical conference and school of young scientists "Science and Education for sustainable development"], 2013, Ch. 3, pp. 8-13 (in Russ.).

3. Gadzhiev G.G., Vasin A.Ya., Anosova E.B. Influence of explosive groups on fire and explosion hazard of organic compounds, Uspekhi v khimii i khimicheskoi tekhnologii [Achievements in chemistry and chemical technology], 2014, Vol. 28, № 2 (151), pp. 53-56 (in Russ.).

4. GOST 12.1.044-89* (ISO 4589-84). SSBT. Fire and explosion hazard of substances and materials. Nomenclature of indices and methods of their determination. (in Russ.).

5. Calculation of the main indicators of fire-and-explosion hazard of substances and materials: rukovodstvo, M.: VNIIPO, 2002. 77 pp (in Russ.).

6. Anosova E.B., Vasin A.Ya., Lyashenko S.M., Marinina L.K., Gadzhiev G.G. Thermal stability and fire-and-explosion hazard of products and semi-products of synthesis of medicines, Pozharnaya opasnost' [Fire Hazard], 2016, № 1, pp. 163-168 (in Russ.).

7. Kissindzher G.E. Reaction kinetics in differential thermal analysis, Analiticheskaya khimiya [Anal. Chem.], 1957, Vol.29 (11), pp. 1702–1706.

8. Gadzhiev G.G., Vasin A.Ya., Matveev A.A. Sensitivity to impact of luminol, its nitro-derivatives and paradinitrosobenzene, Uspekhi v khimii i khimicheskoi tekhnologii [Achievements in chemistry and chemical technology], 2016, Vol. ХХХ, № 8, pp. 21-24 (in Russ.).